Table 1. Thermogravimetric analysis results corresponding to the post-industrial waste PLA, commercial conductive filament, and the three bespoke filaments produced using different amounts of poly(ethylene succinate). Highlighting the average onset temperature, average final mass and the conductive filler content of the filament.

| Filament | Average Onset T (°C) | Average Final Mass (wt%) | Filler Content (wt%) |
| --- | --- | --- | --- |
| Base PLA | 305 ± 5 | 3 ± 2 | - |
| Commercial | 304 ± 2 | 24 ± 2 | 21 ± 3 |
| PES 10% | 247 ± 2 | 31 ± 1 | 28 ± 3 |
| PES 12.5% | 243 ± 3 | 31 ± 1 | 28 ± 3 |
| PES 15% | 228 ± 2 | 28 ± 4 | 25 ± 5 |

Table 2. Comparisons of the calculated peak-to-peak separations (ΔEp), heterogeneous electron transfer (k0obs) and electrochemically active area (Ae) for the filaments used in this work. Calculated using cyclic voltammetry (5.0-300 mV s-1) in a solution of ferrocenemethanol (1 mM in 0.1 M KCl), with a nichrome wire counter electrode and Ag|AgCl reference electrode.

|  | Filament | ΔEp (V) | k0obs (cm s-1) | Ae (cm2) |
| --- | --- | --- | --- | --- |
| Non-Activated | C-PLA/CB | 0.157 ± 0.038 | (1.03 ± 0.31) x 10-3 | 0.019 ± 0.007 |
|  | 10% PES | 0.102 ± 0.020 | (2.05 ± 0.82) x 10-3 | 0.079 ± 0.002 |
|  | 12.5% PES | 0.105 ± 0.021 | (1.99 ± 0.79) x 10-3 | 0.070 ± 0.002 |
|  | 15% PES | 0.100 ± 0.021 | (2.11 ± 0.85) x 10-3 | 0.074 ± 0.005 |
| NaOH + EChem Activated | C-PLA/CB | 0.160 ± 0.029 | (1.10 ± 0.25) x 10-3 | 0.084 ± 0.001 |
|  | 10% PES | 0.085 ± 0.016 | (2.48 ± 1.08) x 10-3 | 0.130 ± 0.003 |
|  | 12.5% PES | 0.084 ± 0.019 | (2.45 ± 1.00) x 10-3 | 0.147 ± 0.006 |
|  | 15% PES | 0.086 ± 0.017 | (2.44 ± 1.07) x 10-3 | 0.155 ± 0.004 |

Table 3. Comparison of the electroanalytical detection of caffeine in phosphate buffer (pH = 5.8) for the commercial PLA/CB filament and the recycled filaments with 10% PES, both activated and non-activated. Highlighting the linear dynamic range (LDR), sensitivity, limit of detection (LOD), limit of quantification (LOQ) and relative standard deviation (RSD).

|  | Electrode | LDR (µM) | Sensitivity (µA µM-1) | LOD (µM) | LOQ (µM) | RSD (%) |
| --- | --- | --- | --- | --- | --- | --- |
| Non-Activated | C-PLA/CB | 50-300 | 0.036 ± 0.001 | 14.6 | 48.7 | 4.37 |
|  | 10% PES | 1.0-500 | 0.043 ± 0.001 | 0.27 | 0.88 | 3.60 |
| NaOH + EChem Activated | C-PLA/CB | 50-300 | 0.039 ± 0.001 | 13.4 | 44.6 | 3.48 |
|  | 10% PES | 1.0-500 | 0.055 ± 0.001 | 0.23 | 0.76 | 3.14 |

Table 4. Caffeine levels found in real and spiked tea and coffee samples (n=3) using the activated 10% PES recycled filament.

|  | Caffeine Added (M) | Caffeine Found (M) | Recovery (%) |
| --- | --- | --- | --- |
| Earl Grey Tea | - | 2.59 x 10-6 | - |
|  | 3.00 x 10-6 | 2.95 x 10-6 | 98.5 |
|  | 5.00 x 10-6 | 5.14 x 10-6 | 103 |
|  | 1.00 x 10-6 | 9.88 x 10-6 | 98.8 |
| Arabica Coffee | - | 1.50 x 10-5 | - |
|  | 2.00 x 10-5 | 2.02 x 10-5 | 101 |
|  | 3.00 x 10-5 | 2.90 x 10-5 | 96.7 |
|  | 1.00 x 10-4 | 1.02 x 10-4 | 102 |