Tables

Table 1. Thermal properties of the recycled filament produced by different processing methods.

| Production Method | Melt Flow Index (g/10 min) | Onset Temperature (°C) | Filler Content (wt%) |
| --- | --- | --- | --- |
| Granulation | 5.73 ± 0.49 | 307 ± 2 | 1.71 ± 0.94 |
| Ball-Milling | 10.2 ± 0.3 | 309 ± 3 | 2.15 ± 0.32 |
| Solvent Mixing | 6.99 ± 0.32 | 308 ± 2 | 2.49 ± 1.06 |
| Thermal Mixing | 7.16 ± 0.36 | 307 ± 5 | 0.67 ± 0.31 |

Table 2. Thermal properties of the commercial filament, and the recycled filament produced by thermal mixing over different cycles.

| Non-conductive Iteration | Melt Flow Index (g/10 min) | Onset Temperature (°C) | Filler Content (w%) |
| --- | --- | --- | --- |
| Commercial PLA | 4.16 ± 0.04 | 305 ± 5 | 0 |
| Iteration 1 | 7.16 ± 0.36 | 307 ± 5 | 0.67 ± 0.31 |
| Iteration 2 | 17.4 ± 0.1 | 307 ± 1 | 1.71 ± 0.84 |
| Iteration 3 | 29.6 ± 0.8 | N/A | N/A |

Table 3. Electrochemical and electroanalytical properties of the different cell iterations. Highlighting the resistance across the AME connection length, the heterogeneous electrochemical rate constant (k0), the real electrochemical surface area (Ae), sensitivity for acetaminophen determination, limit of detection for acetaminophen, and the recovery % from a real pharmaceutical sample.

| Non-conductive Filament | Conductive Filament | AME Resistance (kΩ) | k0 (cm2 s-1) | Ae (cm2) | Sensitivity (µA µM-1) | LOD (µM) | Recovery (%) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Commercial | Commercial | 1.15 ± 0.17 | 2.5 ± 0.2 | 0.075 ± 0.01 | 22.3 ± 0.7 | 4.5 ± 0.9 | 97 ± 5 |
| Recycled - 1 | Commercial | 1.17 ± 0.13 | 2.9 ± 0.6 | 0.074 ± 0.02 | 21.5 ± 0.5 | 4.2 ± 1.2 | 99 ± 6 |
| Recycled - 1 | Recycled | 0.68 ± 0.09 | 3.6 ± 0.4 | 0.081 ± 0.01 | 22.4 ± 0.2 | 3.2 ± 0.8 | 95 ± 5 |