Supplementary Data

Cork-based electrochemical sensors obtained by laser-induced graphene: A green alternative for sodium nitrite detection in beverage samples

Beatriz F. Germinarea, Wilson S. Fernandes-Juniorc, Jéssica R. Camargoa, Bruno C. Janegitza,b*

a Laboratory of Sensors, Nanomedicine, and Nanostructured Materials, Federal University of São Carlos, 13604-900, Araras, São Paulo, Brazil

b Center for Sciences and Technology for Sustainability, Federal University of São Carlos, 18052-780, Sorocaba, São Paulo, Brazil

c Institute of Chemistry, University of Campinas, 13083-862, Campinas, São Paulo, Brazil

*Corresponding author: brunocj@ufscar.br (B. C. Janegitz)

Figure S1. Substrates of cork used for pyrolysis, in which (A) 2.0 mm, (B) 3.0 mm, and (C) 5.0 mm

Figure S2. (A) Cyclic voltammograms obtained by C-CO₂PE in 0.1 mol L−1 KCl, varying power from 9.1% (of 50 W) to 10.1% (of 50 W), ν = 50 mV s−1. (B) Cyclic voltammograms obtained by C-CO₂PE in the absence and presence of 1.0 mmol L−1 FcMeOH, in 0.1 mol L−1 KCl, varying printing speed from 60 to 90 mm s-1, ν = 50 mV s−1. (C) Cyclic voltammograms obtained by C-CO₂PE in the absence and presence of 1.0 mmol L−1 FcMeOH, in 0.1 mol L−1 KCl, varying laser distance from 7 to 13 mm, ν = 50 mV s−1. (D) Scatter plot of the correlation Ip vs. printing speed (mm s-1). (E) Scatter plot of the correlation Ip vs. laser distance (mm)

Table S1. CO2 laser printing operational parameters of the electrochemical system

| Operational Parameters | Tested Parameters | Chosen Parameters |
| --- | --- | --- |
| Power (% - of 50 W) | 9.1 – 10.1 | 9.7 |
| Printing speed (mm s−1) | 60 - 90 | 80 |
| Laser distance (mm) | 7 - 13 | 9 |
| Cutting speed (mm s-1) | 10 | 10 |

Figure S3. (A) Cyclic voltammograms obtained by C-CO₂PE with 0.3 mol L-1 sodium citrate in the absence (dash line) and presence of 1.0 mmol L−1 FcMeOH (blue line), in 0.1 mol L−1 KCl, ν = 50 mV s−1. (B) Cyclic voltammograms obtained by C-CO₂PE with waterproofing spray in the absence (dash line) and presence of 1.0 mmol L−1 FcMeOH (blue line), in 0.1 mol L−1 KCl, ν = 50 mV s−1. (C) Cyclic voltammograms obtained by C-CO₂PE with waterproofing spray and 0.3 mol L-1 sodium citrate, respectively, in the absence (dash line) and presence of 1.0 mmol L−1 FcMeOH (blue line), in 0.1 mol L−1 KCl, ν = 50 mV s−1. (D) Cyclic voltammograms obtained by C-CO₂PE with 0.3 mol L-1 sodium citrate and waterproofing spray, respectively, in the absence (dash line) and presence of 1.0 mmol L−1 FcMeOH (blue line), in 0.1 mol L−1 KCl, ν = 50 mV s−1

Figure S4. (A) Cyclic voltammograms obtained by C-CO₂PE in the presence of 1.0 mmol L−1 FcMeOH (blue line) and 1.0 mmol L−1 [Fe(CN)₆]³⁻/⁴⁻ (black line), in 0.1 mol L−1 KCl, ν = 50 mV s−1. (B) Cyclic voltammograms obtained by C-CO₂PE in presence of 1.0 mmol L−1 FcMeOH (red line), 1.0 mmol L−1 FcMeOH with HCl (pH 2.0) (blue line), and 1.0 mmol L−1 FcMeOH with HNO3 (pH 2.0) (black line), in 0.1 mol L−1 KCl, ν = 50 mV s−1. (C) Cyclic voltammograms obtained by C-CO₂PE in the presence of 1.0 mmol L−1 [Fe(CN)₆]³⁻/⁴⁻ (red line), 1.0 mmol L−1 [Fe(CN)₆]³⁻/⁴⁻ with HCl (pH 2.0) (blue line), and 1.0 mmol L−1 [Fe(CN)₆]³⁻/⁴⁻ with HNO3 (pH 2.0) (black line), in 0.1 mol L−1 KCl, ν = 50 mV s−1

Figure S5. Schematic representation of the redox behavior of FcMeOH, illustrating the oxidation at the iron center of the ferrocene unit, where the Fe(II) is converted to Fe(III), leading to the formation of ferricenium methanol

Figure S6. EDS data of the (A) raw cork, (B) waterproofed cork, and (C) pyrolyzed electrode surface

Figure S7. (A) Thermogravimetric analysis (TGA) of the waterproofed cork (red line), and pyrolyzed electrode (blue line). (B) Derivative thermogravimetry (DTG) of the pyrolyzed electrode (blue line), and (C) waterproofed cork (red line)

Figure S8. (A) Square wave voltammograms obtained by C-CO₂PE in the absence (dash line) and presence (solid line) of 1.0 mmol L−1 sodium nitrite, in 0.1 mol L−1 phosphate buffer (pH 7.0). (B) Differential pulse voltammograms obtained by C-CO₂PE in the absence (dash line) and presence (solid line) of 1.0 mmol L−1 sodium nitrite, in 0.1 mol L−1 phosphate buffer (pH 7.0). (C) Comparison of current variation vs techniques (SWV and DPV) in the presence of 1.0 mmol L−1 sodium nitrite, in 0.1 mol L−1 phosphate buffer (pH 7.0). (D) Square wave (blue line) and differential pulse (red line) voltammograms obtained by C-CO₂PE in the absence (dash line) and presence (solid line) of 1.0 mmol L−1 sodium nitrite, in 0.1 mol L−1 phosphate buffer (pH 7.0). DPV parameters: step = 5 mV; modulation amplitude = 50 mV; modulation time = 50 ms; ν = 30 mV s−1. SWV parameters: pulse amplitude = 20 mV; potential step = 5 mV; frequency = 6 Hz, and ν = 30 mV s−1

Figure S9. (A) Square wave voltammograms obtained by C-CO₂PE in the presence of 1.0 mmol L−1 sodium nitrite, in 0.1 mol L−1 phosphate buffer (pH 7.0) varying amplitude from 10 to 100 mV. (B) Scatter plot of the correlation Ip vs. Pulse amplitude (mV). (C) Square wave voltammograms obtained by C-CO₂PE in the presence of 1.0 mmol L−1 sodium nitrite, in 0.1 mol L−1 phosphate buffer (pH 7.0) varying potential step from 1 to 10 mV. (D) Scatter plot of the correlation Ip vs. Potential step (mV). (E) Square wave voltammograms obtained by C-CO₂PE in the presence of 1.0 mmol L−1 sodium nitrite, in 0.1 mol L−1 phosphate buffer (pH 7.0) varying frequency from 5 to 30 Hz. (F) Scatter plot of the correlation Ip vs. Frequency (Hz)

Table S2. Operational parameters for SWV technique optimization, in the presence of 1.0 mmol L−1 sodium nitrite, in 0.1 mol L−1 phosphate buffer (pH 7.0)

| Operational Parameters | DPV | Tested Parameters SWV | Chosen Parameters SWV |
| --- | --- | --- | --- |
| Modulation amplitude (mV) | 50 | - | - |
| Pulse amplitude (mV) | - | 10 - 100 | 70 |
| Potential step (mV) | 5 | 1 - 10 | 3 |
| Frequency (Hz) | - | 5 - 30 | 5 |
| Modulation time (ms) | 50 | - | - |

Figure S10. Evaluation of the selectivity and interference tolerance of the C-CO₂PE sensor for sodium nitrite detection in the presence of common interferents, including KCl, NaCl, C₆H₈O₇ (citric acid), Na₂SO₃, and CaCl₂. The red dashed line indicates the current response to sodium nitrite (SN), serving as a reference for comparison.

Figure S11. (A) Square wave voltammograms obtained by C-CO₂PE in the presence of 1.0 mmol L−1 sodium nitrite, in 0.1 mol L−1 phosphate buffer (pH 7.0), in 5 different scans. (B) Square wave voltammograms obtained by C-CO₂PE in the presence of 1.0 mmol L−1 sodium nitrite, in 0.1 mol L−1 phosphate buffer (pH 7.0), in 5 different electrodes