Reviewer #1

Review Report Form

Open Review

(x) I would not like to sign my review report
( ) I would like to sign my review report

English language and style

( ) Extensive editing of English language and style required
( ) Moderate English changes required
(x) English language and style are fine/minor spell check required
( ) I don't feel qualified to judge about the English language and style

|  | Yes | Can be improved | Must be improved | Not applicable |
| --- | --- | --- | --- | --- |
| Does the introduction provide sufficient background and include all relevant references? | ( ) | (x) | ( ) | ( ) |
| Are all the cited references relevant to the research? | (x) | ( ) | ( ) | ( ) |
| Is the research design appropriate? | ( ) | (x) | ( ) | ( ) |
| Are the methods adequately described? | ( ) | (x) | ( ) | ( ) |
| Are the results clearly presented? | ( ) | (x) | ( ) | ( ) |
| Are the conclusions supported by the results? | (x) | ( ) | ( ) | ( ) |

Comments and Suggestions for Authors

The authors reported a novel flexible supercapacitor device from a polyethylene terephthalate substrate, reused from beverage bottles, and a conductive ink based on carbon black (CB) and cellulose acetate (CA). As a result, the highest capacitance value for the device with the 66.7/33.3 wt% CB/ CA in a basic H2SO4 solution could reach 135.64 F g−1, and the values of 2.45 Wh Kg−1 for specific energy and around 1000 W Kg−1 for specific power. Overall, the work is of some novelty. But before its further consideration, some issues need to be verified.

- In the introduction, some typical supercapacitors based on carbon materials should be cited: Advanced Functional Materials 2015, 25 (47), 7381-7391. Journal of Materials Chemistry A 2018, 6 (41), 20254-20266; Advanced Energy Materials 2019, 9 (47), 1902915. Energy Storage Materials 2018, 13, 96-102

R: We appreciate the suggestion and the proposed works are added to the introduction, when pertinent to the discussion.

- The carbon black (CB) and cellulose acetate (CA) should be characterized by XRD and SEM.

R: We agree with the reviewer suggestion that XRD would be an interesting analysis. However, the only equipment we have access to is under maintenance, and there is no scheduled date for when it will work again. SEM images of the final ink without CA, without CB, and in its completeness were performed and the discussion was redone.

- In Fig. 2c, some peaks occur at the CV curve, please explain.

R: According to the literature, these peaks could be associated with the redox process of surface electroactive functional groups, mainly ketones, phenols, and carboxylic groups [1, 2]. Also, the effects of such processes would require extensive and proper research, as they can provoke pseudocapacitive behavior, even being unstable in nature [1, 3]. Also, we noted a discrepancy in the data presentation: the voltammetries regarded in Figure 2A to C were performed at 10 mV s-1. The appropriate corrections were made in the text.

References

[1] M. Toupin, D. Bélanger, I.R. Hill, D. Quinn, Performance of experimental carbon blacks in aqueous supercapacitors, Journal of power sources, 140(2005) 203-10.

[2] E. Frackowiak, F. Beguin, Carbon materials for the electrochemical storage of energy in capacitors, Carbon, 39(2001) 937-50.

[3] B.E. Conway, Electrochemical supercapacitors: scientific fundamentals and technological applications: Springer Science & Business Media; 2013.

- The rate capacity should be measured at different current densities.

R: The rate capacity of CB/CA was calculated and the discussion was expanded.

Submission Date: 21 April 2022

Date of this review: 27 Apr 2022 08:26:26

Reviewer #2

Review Report Form

Open Review

(x) I would not like to sign my review report
( ) I would like to sign my review report

English language and style

( ) Extensive editing of English language and style required
( ) Moderate English changes required
( ) English language and style are fine/minor spell check required
(x) I don't feel qualified to judge about the English language and style

|  |  | Yes | Can be improved | Must be improved | Not applicable |
| --- | --- | --- | --- | --- | --- |
| Does the introduction provide sufficient background and include all relevant references? |  | ( ) | (x) | ( ) | ( ) |
| Are all the cited references relevant to the research? |  | ( ) | (x) | ( ) | ( ) |
| Is the research design appropriate? |  | ( ) | (x) | ( ) | ( ) |
| Are the methods adequately described? |  | ( ) | (x) | ( ) | ( ) |
| Are the results clearly presented? |  | ( ) | (x) | ( ) | ( ) |
| Are the conclusions supported by the results? |  | ( ) | (x) | ( ) | ( ) |

Comments and Suggestions for Authors

This paper reports flexible supercapacitor devices using carbon black with cellulose acetate on terephthalate substrates. This paper reveals good capacitance performances using a simple and eco-friendly strategy process. My comments are listed below.

1) The electrochemical performance strongly depends on the structural properties of the used CB. Therefore, I recommend showing the electrochemical performance using different CB to reveal CB(VULCAN) with CA used in this study is an essential finding or not.

R: We appreciate and agree with the reviewer suggestion, but would like to emphasize that this investigation would deviate from the intent of this work. The structural properties of carbon black (CB) vary according to its surface and the synthesis method [1-3], but without further modification of the device, they show similar morphological and structural properties. For example, a study by Mazzaracchio et al. [4] showed that different CB samples exhibited the same onion-like carbon structure. The Raman spectra for the samples showed several moments of similarity, including in the presence of the symmetry defects of the sp2 systems [5]. Another similarity of the different CB, is that they can form agglomerates due to their high specific surface area, and present characteristics of materials with spherical nanometric particles [6]. Given these similarities for different CB samples, we believe that a more interesting approach would not necessarily be the study of different types of CB, but rather to evaluate the fabrication of the material, as already investigated by Toupin et al. [7].

References

[1] P.B. Deroco, R.C. Rocha-Filho, O. Fatibello-Filho, A new and simple method for the simultaneous determination of amoxicillin and nimesulide using carbon black within a dihexadecylphosphate film as electrochemical sensor, Talanta, 179(2018) 115-23.

[2] S. Jebril, L. Cubillana-Aguilera, J.M. Palacios-Santander, C. Dridi, A novel electrochemical sensor modified with green gold sononanoparticles and carbon black nanocomposite for bisphenol A detection, Materials Science and Engineering: B, 264(2021) 114951.

[3] T.A. Silva, A. Wong, O. Fatibello-Filho, Electrochemical sensor based on ionic liquid and carbon black for voltammetric determination of Allura red colorant at nanomolar levels in soft drink powders, Talanta, 209(2020) 120588.

[4] V. Mazzaracchio, M.R. Tomei, I. Cacciotti, A. Chiodoni, C. Novara, M. Castellino, et al., Inside the different types of carbon black as nanomodifiers for screen-printed electrodes, Electrochimica Acta, 317(2019) 673-83.

[5] A. Coccato, J. Jehlicka, L. Moens, P. Vandenabeele, Raman spectroscopy for the investigation of carbon-based black pigments, 46(2015) 1003-15.

[6] Z. Li, J. Zhang, S.J.E.P.L. Chen, Effects of carbon blacks with various structures on vulcanization and reinforcement of filled ethylene-propylene-diene rubber, 2(2008) 695-704.

[7] M. Toupin, D. Bélanger, I.R. Hill, D. Quinn, Performance of experimental carbon blacks in aqueous supercapacitors, Journal of power sources, 140(2005) 203-10.

2) There is no detailed experimental information on the analysis of flexibility relating to their electrochemical performance.

R: We appreciate the suggestion and the proper experimental procedure was added to the experimental section.

Submission Date: 21 April 2022

Date of this review: 02 May 2022 03:59:05