Development of disposable and flexible supercapacitor based on carbonaceous and ecofriendly materials

Giovanni G. Daniele1, Daniel C. de Souza1, Luiz O. Orzari1,2, Rodrigo V. Blasques1,2, Rafael L. Germscheidt3, Emilly C. da Silva4, Leandro A. Pocrifka4, Juliano A. Bonacin3, Bruno C. Janegitz1.

1Laboratory of Sensors, Nanomedicine and Nanostructured Materials, Federal University of São Carlos, Araras, Brazil, 13600-970

2Department of Physics, Chemistry, and Mathematics, Federal University of São Carlos, Sorocaba, São Paulo, Brazil, 18052-780

3Institute of Chemistry, University of Campinas (UNICAMP), 13083-859, Campinas, São Paulo, Brazil.

4Laboratory of Electrochemistry and Energy (LEEN), Chemistryl Graduate Program of Federal University of Amazonas (UFAM), 69067-005, Manaus, Amazonas, , Brazil

Graphical Abstract

EM PREPARO

Abstract

A novel flexible supercapacitor device was developed from a polyethylene terephthalate substrate, reused from beverage bottles, and a conductive ink based on carbon black (CB) and cellulose acetate (CA). The weight composition of the conductive ink was evaluated in order to determine the best mass percentage ratio between CB and CA in terms of the capacitive behavior. The evaluation was performed by using different electrochemical techniques: cyclic voltammetry, obtaining the highest capacitance value for the device with the 66.7/33.3 wt% CB/ CA in a basic H2SO4 solution, reaching 135.64 F g-1. The device was applied in potentiostatic charge/discharge measurements, achieving values of 2.45 Wh Kg-1 for specific energy and around 1000 W Kg-1 for specific power. Therefore, corroborated with electrochemical impedance spectroscopy essays, the relative low price proposed device presented a suitable performance for application as supercapacitors, being manufactured from reused materials, contributing to the energy storage field enhancement.

Keywords: Disposable device; Supercapacitor; Carbon material; Carbon Black; Cellulose Acetate.

1. Introduction

The energy issue has been one of the great discussions around the world due to the depletion of fossil fuels, which has attracted the search for new sources of energy conversion and storage. This issue arises from the constant demand for fast, economically efficient and ecologically correct technological devices, to meet the world growing population desires for frequent information [1-3]. In such industry, electrochemical energy conversion systems function as key technologies, allowing the management of renewable energy while diminishing the pollution caused by other sources, such as the greenhouse effect [2]. While common batteries are widely researched, discussed and employed, especially in electric or hybrid vehicles [2, 4, 5], they have some lifetime and power issues, like low power density, requiring longer charge and/or discharge time, capacitors can operate at short charge-discharge times (<0.1 s) resulting in low production and maintenance costs. As demonstrated by Libich et al. [1], electrochemical capacitors, also known as supercapacitors, presents high energy densities, close to that of batteries, while also bringing the higher power densities of pure metal capacitors. Besides, they have been gaining prominence due to relative low cost, renewable materials usage, and high-efficiency energy storage capability [6-8]. It is also known that even at high discharge rates, their efficiency and reversibility exceed 90% [9, 10], further suggesting that supercapacitors could be ideal for renewable energy storage.

Hence, technological development is requesting new applications and, in this scenario, flexible supercapacitors have attracted great interest in the industry. This class of materials meets the technological requirements for advances in the field of wearable, compact, and portable electronics, such as flexible displays on phones, health tracking devices, computers, televisions, electronic textiles, artificial electronic skin, and distributed sensors [11-13]. Moreover, the key challenge for the conception of the commercial supercapacitors is the development of devices with excellent mechanical flexibility and adjustable dimensions along with decreasing production cost [14, 15].

In this context, various carbon materials have been proposed as electrode materials for electric double layer capacitors, and among them, carbon black (CB) stands out due to the structure of the graphitic domains in the concentric particles, ensuring adequate electrical conduction, combined with the porosity of the carbonaceous material, having the capacity to store energy in the form of electrical charges [16-18].

In addition, CB has the ability to form stable dispersions polymeric matrices [19], being applied for the fabrication of 2D printed electrodes, using a technology known as screen-printing [20, 21]. This technology consists in the application of a conductive ink over a screen, delimiting the form of the desired electrodes on the surface of an inert substrate. This conductive ink is conventionally made by the dispersion of electrically conductive particles on a polymeric matrix, and, among renewable options, cellulose acetate (CA) could be an interesting choice as it is biodegradable polymer of biological sources, synthesized from cellulose with relative low production cost [22-24]. The literature also presents screen-printed systems as possible disposable materials [25-27], due to their reduced production cost, when compared to conventional electrodes. This, however, also demands an ecofriendly inert substrate, such as reusable beverage bottles (polyethylene terephthalate, PET) [25], and sandpapers [28]; or recyclable materials, as paper [29], waterproof paper [30], fiberboard [31] and polyvinyl chloride [32].

The selection of electrode materials directly affects the electrochemical performance, physical properties and further applications of the device. Therefore, the development of flexible supercapacitors is very important for different technologies, making essential the search for cheaper and renewable materials, with optimal operational parameters. In this work we propose the development of a disposable and flexible supercapacitor, using the screen-printing technique, with a conductive and lab-made ink of CB and CA, deposited over a PET substrate, presenting and discussing its behaviors, characteristics and efficiencies in different pH medias.

2. Experimental

2.1. Reagents and solutions

All chemicals used in this work were purchased from Sigma-Aldrich (Germany) and/or Fluka (Brazil), with analytical grade. In addition, all aqueous solutions used for electrochemical characterizations, including the supporting electrolytes: sulfuric acid (H2SO4), potassium hydroxide (KOH) and sodium sulfate (Na2SO4); were prepared by an ultrapure water system Synergy® (type 1) from Merck Millipore (Merck Group, USA), with resistivity > 18 MΩ cm. For ink preparation, VULCAN® XC-72 conducting carbon black (CB) powder was provided by CABOT, and the Polyethylene Terephthalate (PET) substrates were obtained by reusing different beverage bottles.

2.2. Apparatus

The CB-based electrodes were elaborated and assembled with the aid of Silhouette Studio 4.4® (Silhouette, Brazil) software, used to elaborate the capacitor mask design, and command the Silhouette Cameo 3® cutting machine (Silhouette, Brazil). For the ink preparation, a magnetic stirrer and heater (Biomixer AM-10), and an ultrasonic bath purchased from (Cristófoli, Brazil) were used.

The electrochemical characterizations were performed in a Potentiostat/Galvanostat (Metrohm, Autolab/PGSTAT204) with an expansion module for Electrochemical Impedance Spectroscopy (EIS) FRA32M performance. Managed by NOVA 2.1.4 software, at the open circuit potential (OCP) with sine wave type, 10 mV amplitude, in the frequency range of 0.1 MHz to 10 mHz. Morphological characterizations were conducted by (Scanning Electronic Microscope) SEM images obtained in a Vega-3 LMU Tescan electronic microscope, in 10kV voltage acceleration and 50P low vacuum mode. The electrochemical impedance spectroscopy (EIS) data was obtained in three different 1.0 mol L-1 electrolytes: H2SO4, KOH and Na2SO4. Data was obtained with the following parameters: applied potential of corresponding to the OCP of each system, obtained after 300 s stabilization, being -26 mV for H2SO4 and -56 mV for KOH; potential amplitude of 10 mV, sine waves type throughout all analysis, and 10 frequency increments per decade, in the range of 1.0×105 to 1.0×10-2 Hz.

2.3 Production of the ink and manufacture of the disposable electrodes

To guarantee optimal ink formulation and materials dispersion, two solvent solutions were prepared, with a mixture of N, N-Dimethylformamide (DMF) and acetone (ACE) of distinct volume %. The solvent to best dispersed CA had a 52.5/47.5% ratio, while the solvent that better dispersed CB, presented a ratio of 42.4/57.6%. The CA dispersion was prepared by adding 250 mg of the acetate in mentioned solvent, subsequently stirring it for 10 min at 60 ºC. Meanwhile, the CB dispersion was produced by adding a desired amount of CB to the corresponding DMF/ACE mixture and placing it in an ultrasonic bath, for 30 min, to enhance homogenization. Finally, these two dispersions were mixed together in different proportions, following another ultrasonic bath for 30 min. After, the final dispersion was magnetically stirred for 10 min, finishing the conductive ink. The final CB:CA proportions are presented in Table 1:

| Table 1 – CB/CA proportions at the different prepared inks |  |  |  |
| --- | --- | --- | --- |
| Formulation Nº | CB (mg) | CA (mg) | CB/CA% (w/w) |
| 1 | 125 | 250 | 33.3/66.7 |
| 2 | 250 | 250 | 50.0/50.0 |
| 3 | 375 | 250 | 60.0/40.0 |
| 4 | 500 | 250 | 66.7/33.3 |

To assemble the electrodes systems, the polyethylene terephthalate (PET) substrates, obtained by reusing beverage bottles, were cut, properly washed and polished to enhance ink adhesion. After, adhesive paper sheets were cut by the cutting machine with a proper design, based on three-electrodes system. These adhesive masks were attached to the PET surface, and the ink was applied over them. After 10 min of drying, a second ink layer was produced, and it was left to dry at 19 °C. After, the paper masks were removed and the system was ready to use. Figure 1 illustrates the whole process.

Figure 1. Experimental procedure representation: (1) elaboration of the CB and CA base dispersions; (2) homogeneous ink preparation; (3) electrode assemble by screen printing technique over PET substrates; (4) finalized capacitor electrode ready for (5) electrochemical analyses

3. Results and discussion

3.1 Electrochemical and morphological characterizations

In order to understand the CB/CA ink capacitive behavior, different characterization procedures should be investigated. Therefore, the first electrochemical study performed was a profile determining cyclic voltammetry (CV) technique, aiming to analyze and compare the four different ink formulations, based on each specific capacitance (SC) response at different electrolytes: an acid (H2SO4), a saline (Na2SO4) and a basic (KOH) media, with respective 1.0 mol L-1 concentration. Properties such as active surface area, porosity and conductivity are crucial points in the development of electrochemical capacitors, and this is directly influenced by the amount of carbonaceous material used [33]. Thus, the voltammetric profiles in Figures 2A (acidic), 2B (saline) and 2C (alkaline), obtained by different CB/CA compositions, demonstrates that, majorly, there is a predominance of the capacitive current, even though a few electrodes presented redox interactions, limiting their use as capacitive devices. This highly capacitive behavior indicates that the materials perform energy storage through an expansion in the electrical double layer, storing charges directly on the double layer [34]. This class of devices is commonly called an expanded double-layer capacitor (EDLC) [35, 36].

This observed characteristic profile is possibly caused by the presence of discrete pores in the proposed electrodes, where carbon atoms of the CB are compacted at the channels edges. All Figure 2 voltammograms demonstrates an approximately rectangular voltametric profile, a characteristic near-ideal capacitor behavior, which is justified by diffusion processes. Also, this study shows that the variation of current flowing through the circuit increases linearly with the CB concentration, indicating that the larger amounts of CB enhance the capacitive behavior. Probably, this functions by the increase in number of active sites, due to the higher atomic density, contributing in the double layer formation process [36]. Herewith, the ink containing the highest quantity of CB (66.7/33.3%, w/w) was chosen to continue this work.

Figure 2. Cyclic voltammograms of different CB/CA formulations: 33.3/66.7 (black), 50.0/50.0 (red), 60.0/40.0 (blue) and 66.7/33.3% (pink); in (A) 1.0 mol L-1 H2SO4, (B) 1.0 mol L-1 KOH and (C) 1.0 mol L-1 Na2SO4; n = 1.0 mV s-1 (D) SC vs scan rate plots for 66.7/33.3% CB/CA at equimolar 1.0 mol L-1 H2SO4 (▲); Na2SO4 (●) and KOH (■) solutions

Thus, with the previously charge data acquisition aided for CV technique, the resultant charge data influence, at each electrolyte, with different scan rates (n), guided by SC values would be estimated by the Equation 1.:

|  | SC=∆Qm×∆V | (1.) |
| --- | --- | --- |

where SC is expressed in (F g-1); ΔQ is the charge variation in terms of C s-1; m is the electrode mass, which were estimated around 0.134 mg for the chosen formulation; and ΔV is the working potential used, represented in V. Therefore, the resultant SC values vs different n (mV s-1) is shown in Figure 2D, for each electrolyte. The resultant dispersion, in general, presented a capacitance decrease with the increasing of n. This was an expected behavior, especially because of the velocity of surface formation processes, including surface resistance, double layer thickness and charge diffusion as well, that are all processes in progress during data collection. It is important to highlight, however, that the CB/CA electrode demonstrated a more stable SC vs n curve in the acidic electrolyte, with a decrease of only 75%, when compared to the other media (93% for KOH and 87% for Na2SO4).

EIS technique configures a very important tool for mapping processes at electrode interface, which may include redox reactions, adsorption and forced mass transfer processes. It provides responses in function of the relation between frequency and a given potential, in contrast with the most used electroanalytical methods. This technique is useful to electrochemical devices, especially energy storage systems, like batteries, capacitors and supercapacitors, especially as they need more comprehensive information about resistivity and charge transfer of electrodes materials.

In this study (Figure 3A), it was observed that the acidic profile presents a low frequency region almost in parallel to the imaginary axis, which characterizes an ideal capacitive behavior due to minimal material resistance effects are being observed in lower frequencies. This could imply that the double-layer ion transport has ceased, achieving equilibrium, and only dielectric behavior is being observed [37, 38]. This behavior is described by a [R(RQ)C] equivalent circuit. For KOH medium, the electrode shows a profile containing deviations from ideal capacitor behavior, especially by the formation of two semicircles, probably caused by proper material hybrid capacitive/resistive behavior, better described with the [R(RQ)([RW]C)] equivalent circuit. The first semi-circle is, potentially, due to the device geometry [37], while the second could be originated from the surface redox reactions, as presented in Figure 2B. The literature proposes a few explanations of such reactions: The device could be functionalized by the basic electrolyte, adsorbing hydroxyl ions [39] or given rise to pseudocapacitance by oxygen involved redox processes [40].

Each system was then evaluated for its behavior against the OCP values used in EIS, and the profiles are presented in Figure 3B. As can be noted, both presented a characteristic voltammograms with only capacitive current generation. It could also be highlighted that the acidic system is considerably of a more rectangular shape than the basic one, implying a higher energy storage capability. By increasing the number of cycles in CV to 100, the capacitance retention of each system was evaluated against previously obtained data (100%). In alkaline solution (Figure 3C), the device rapidly presented an increase of capacitive current, equivalent to 130%, but quickly dropped to around 65%. The device then linearly increased the retention to 74% after all scans. This behavior implies in a non-stable surface. In acidic solutions (Figure 3D), the retentions started at around 80%, increasing to 84% after all cycles, suggesting higher stability. This data also corroborates with the use o acidic electrolytes to proper employ the proposed device as supercapacitor.

Figure 3. (A) Nyquist diagrams for H2SO4 (■) and KOH (●). (B) Cyclic voltammograms obtained in OCP by 66.7/33.3% CB/CA electrode, in equimolar 1.0 mol L-1 H2SO4 (▬) and KOH (▬); n = 10 mV s-1. Capacitance retention dispersion plots of 100 cycles in (C) 1.0 mol L-1 KOH and (D) 1.0 mol L-1 H2SO4.

Morphological characterizations were required to better understand the proposed material and confirm its electrochemical behavior. Therefore, SEM was carried out for the optimal 66.7/33.3% (w/w) CB/CA ink and the resulting image is presented in Figure 4. It is possible to observe the roughness of the whole surface, with pores distributed throughout the film structure, corroborating with the data discussed previously. Also, the carbonaceous structure is observed, proving a homogeneous distribution of CB. This active distribution of amorphous carbon can be associated with the overall material conductivity.

Figure 4.  SEM images of the 66.67% CB/CA ink at (A) 500× and (B) 10000× magnification

3.3 Potentiostatic Charge/Discharge evaluation

Charge and discharge tests were carried out by performing potentiostatic charge/discharge technique (PCD). These tests are extremely important for a more complex analysis about the devices behavior in an applied situation, by inserting the material under a charging and discharging phenomenon, at distinct current density (CD) values, through time. Thus, it is expected to observe profiles with a triangular shape, that results from the device double layer charge/discharge response. This process depends on the charges movement rate through each material gram. As such, this behavior is principally affected by resistance and diffusion layer processes at electrolyte/electrode interface.

Therefore, the CD values were selected arbitrarily at PCD procedure and the chosen values were: 0.5, 1.0, 2.0, 3.0 and 4.0 A g-1, and their resulting profiles for the CB ink are presented in Figure 5. In Figure 5A, the charge and discharge relationship at H2SO4 presented the discussed triangular profile, as expected for a capacitor. Nonetheless, plot lines inclination suggested a smooth charges transition. This type of profile indicates a closer relation with supercapacitors behavior, which conventionally shows a relatively high energy and power densities with smooth rate transitions.

Hereupon, profiles for Na2SO4 presented in Figure 5B, also demonstrated the triangular tendency through CD rising, but started to show some alterations in shape resolution, probably due to process alterations at the double layer, like a pseudocapacitance rising phenomenon [41]. This tendency is accentuated at KOH profiles (Figure 5C), specially at discharge lines, where its definition intensifies the pseudocapacitance growth hypothesis, added to a possible decrease in activity, due to the higher pH, since water-based electrolytes were used [42, 43]. With this, it is possible to conclude that the charge and discharge time increases with at saline and alkaline solutions, while the acidic electrolyte seems to have more attractive features for a supercapacitor, including a flatter profile and lower PCD time.

Figure 5. E vs t plots of CB/CA PCD profiles in 1.0 mol L-1 (A) H2SO4; (B) Na2SO4; (C) KOH, at different CD values: 0.5; 1.0; 2.0; 3.0 and 4.0 A g-1. (D) SP vs SE (Ragone plots) for CB/CA in different and equimolar 1.0 mol L-1 electrolytes: H2SO4 (▲), Na2SO4 (●) and KOH (■); (E) Dispersion plot of PCDs SC vs different current densities (0.5, 1.0, 2.0, 3.0 and 4.0 A g-1) for CB/CA in different and equimolar 1.0 mol L-1 electrolytes: H2SO4 (▲), Na2SO4 (●) and KOH (■); (F) Capacitor efficiency, in equimolar 1.0 mol L-1 H2SO4 (▲), Na2SO4 (●) and KOH (■), for CB/CA devices

3.2 Energy and Power density calculations

Energy and power density values present a relevant form to cross and compare data between different energy storage devices, especially through the Ragone plot (Figure 5D), which are composed by specific power (SP) and specific energy (SE) magnitudes. Therefore, the Ragone graphic was plotted by utilizing two equations, one for the device specific energy (SE, Equation 2.)

|  | SE=I × Δ V × ∆t2 × m | (2.) |
| --- | --- | --- |

where SPe is expressed in Wh Kg-1; I the PCDs discharge current in A; Δt the discharge time in seconds (s); m the work electrode mass g; ΔV is voltage variation through discharge process in V; and the other is for its specific power (SP, Equation 3.):

|  | SP=I × Δ V2 × m | (3.) |
| --- | --- | --- |

where SPw is in terms of W Kg-1. The graphic obtained by plotting SP vs SE presents a comparison of the electrode performance at different media, and shows a very interesting behavior between the two axes, especially for the acidic medium, which get closer to a storage device behavior, with high SP per SE.

To better understand the SC behavior of the device, obtained by PCD, the SC values were converted with a different SC formula, which considers the proper time data obtained by PCDs essays, expressed by Equation 4.:

|  | SC=I × ∆tm×∆V | 4. |
| --- | --- | --- |

where SC is the PCD SC in terms of F g-1; I is the applied current in terms of A; Δt the discharge time (s); m the work electrode mass (g); and ΔV is the voltage variation through discharge process in V. Herewith, the SC calculated values were plotted against the previously chosen CD values, for each electrolyte studied, as can be seen at Figure 5E.

At low CD values, the saline and alkaline electrolytes presented higher SC values than the acidic one. Although, with the CD increase, this tendency decays and, in general, the acidic medium presented more stability throughout the SC variation. This behavior shows an interesting feature that justifies a supercapacitor-like performance, in sulfuric acid, especially because of its flat and stable PCD profile.

Figure 5F shows the device efficiency plot in function of the selected different current densities, calculated by Equation 5.:

|  | n=DtCt | 5. |
| --- | --- | --- |

where n is the estimated efficiency in percentage (%); Dt is the PCD discharge time in seconds (s); and Ct, the PCDs charge time, also in seconds. This plot shows the device efficiency at the selected electrolyte. This is an important indicator to corroborate device performance over a range of current densities. Unlike before, the device present more stable efficiencies at acidic and alkaline media, but with a considerable higher value for the first one. This further justifies previous hypothesis about this device super capacitive behavior. Whereas, saline medium showed a more linear behavior with the previous tests, presenting certain instabilities under the studied current densities, compromising the device in optimized supercapacitor applications.

3.5 Flexibility study

Flexibility is, as discussed previously, an important attribute for capacitors and supercapacitors, enabling the production of different and adaptable technologies. To evaluate it, tests were carried out by twisting the electrode and subsequent collecting its response with CV at 50 mV s-1, with torsions interval of 20 torsions, for a total of 200. This process was repeated twice, with different configuration for data obtention, one with the device still twisted and the other with the device laid flat, to better understand the effect of such strain in the ink. As can be seen in Figures 6A and 6B, both obtained profiles presented stable profiles across all cycles, with little difference between the curved and the flat electrode system, as can be noted in Figure 6C. As the PET substrate has a geometrically curved shape, due to the circumference of beverage bottles, the forced flattering of electrodes puts the ink under increased stress, diminishing the current obtained. Besides that, the electrode shows considerable stability under mechanical stress, effectively working as a flexible device.

Figure 6. Cyclic voltammograms of the flexibility study at (A) curved device and (B) flat device, in 1.0 mol L-1 H2SO4; n = 50 mV s-1. (C) I vs number of torsions dispersion plot for (▲) curved and (●) flat electrodes. Data collected at 0.0 V

Similar supercapacitors were chosen for comparison with the values of specifics capacitance, power and energy, which are comparable to the literature (Table 1). The data collected suggests interesting performance of the developed device in terms of specifics energy and capacitance, implying its use as energy storage device. The majority of the selected works describe different capacitors, micro-capacitors and supercapacitors systems, usually utilizing relative higher-cost materials with complex processes like vapor-liquid-solid chemical vapor deposition [44], and hydrogels synthesis [45]. On the other hand, the proposed work uses a simple synthesis method, while still employing relatively low cost and ecologically friendly materials.

| Table 1. Comparison between this work and others present in literature for supercapacitor characteristics |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Types of cell | Composition | Specific capacitance | Specific power | Specific energy | Works |
| Three electrodes | Highly doped silicon nanowires | 46 µF cm−2 | 1.6 mF cm−2 | Not specified | [44] |
| Two electrodes | N-doped Graphene/PANI hydrogel | 584.7 mF cm−2 | − 0.5 mW cm−2 | ~0.1 mWh cm−2 | [45] |
| Two electrodes | PANI-N/CNT | 341.0 F g−1 | 40.0 W kg−1 | 11.5 Wh kg−1 | [46] |
| Two electrodes | ACTIVATED CARBON-PTFE | 2.1 mF cm−2 | Non specified | Non specified | [21] |
| Two electrodes | PANI-MLG | 110 mF cm−2 | 0.15 mW cm−2 | ~0.01 mWh cm−2 | [6] |
| Two electrodes | PANI/cellulose/Ag | 310.9 F g−1 | 238.2 W kg−1 | 0.7 Wh kg−1 | [13] |
| Two electrodes | PANI-MLG | 451.0 F g−1 | 3610.0 W kg−1 | 17.0 Wh kg−1 | [47] |
| Three electrodes | Vanadium nitride and nickel oxide thin film | 1.85 mF cm-2 | 28 mW cm-2 | 0.7 mWh cm-2 | [48] |
| Two electrodes | IPCN-alkaline carbon metal | 200 F g−1 | Non specified | Non specified | [49] |
| Three electrodes | Carbon Black- cellulose acetate | 313.53 F g−1 | 455.691W kg−1 | 5.84 Wh kg−1 | This work |
|  |  | 168.05 mF cm−2 | 0.24437 mW cm−2 | 0.00313 mWh cm−2 | This work |

Highly doped silicon nanowires: silicon nanowires-based electrodes for micro-capacitor applications, elaborated with highly n and p type doping in silicon nanowires grew with gold catalyst at chemical vapor deposition (CVD) reactor. N-doped Graphene/PANI hydrogel: N type doped PANI hydrogel/graphene oxide (GO) composite electrode synthesized by hydrothermal process, for flexible supercapacitor assemble. PANI-N/CNT: electrode based on activated carbon nanoparticles doped with nitrogen, obtained from PANI nanoparticles pyrolysis for capacitor application. ACTIVATED CARBON-PTFE: Ink-jet printed electrode with an ink formulation obtained by mixing activated carbon powder, polytetrafluoroethylene (PTFE) polymer, ethylene glycol and surfactant. Subsequently printing over a silicon substrate for micro-capacitor applications. PANI-MLG: PANI modified multilayer graphene electrodes. IPCN-alkalyne carbon metal: interconnected porous carbon nanosheets with controllable pore size

4. Conclusion

The production of a flexible supercapacitor electrode was demonstrated in this paper, using a polyethylene terephthalate (PET) substrate. The mass quantity of CA and carbon black were tested in different aqueous media in order to optimize the capacitance response. The device is potentially disposable as it is obtained from eco-friendly and relatively low-cost materials, compared to others employed in electrochemical capacitors development. The optimal composition was achieved with 66.7/33.3 wt% CB/CA, and its storage mechanism is predominantly by the electrical double layer, as evidenced by cyclic voltammetry, presenting an outstanding capacitive behavior on acidic media, demonstrating absence of redox reactions in this condition. In the PCD technique the device presented more defined charge/discharge graphics, leading to more capacitive behaviors in both acidic and basic solutions. In these conditions, specific power of 1000 W Kg-1 in the acidic medium was obtained. Through the EIS technique it was possible to observe a highly capacitive behavior in acidic media and a hybrid capacitive/resistive profile in basic electrolyte. The device also presented 84% capacitance retention after 100 cycles and is quite stable after 200 torsions. All these data suggests that the device is indeed optimal in lower pH systems, but some energy storage can still be obtained in higher pH electrolytes. The proposed device also demonstrated interesting charge-storage capacity and cyclic stability, especially in acidic solutions, affirming its path as an alternative environmentally friendly supercapacitor with simple fabrication.

Acknowledgements

The authors are grateful for the financial support of the Brazilian Funding Agencies. This work was supported in part by Coordenação de Aperfeiçoamento de Pessoal de Nível Superior - Brasil (CAPES) - Financial Code 001, Conselho Nacional de Desenvolvimento Científico e Tecnológico CNPq (NUMBERS) and Fundação de Amparo à Pesquisa do Estado de São Paulo, FAPESP (2017/23960-0, 2017/11986-5, 2019/23342-0).

References

[1] J. Libich, J. Máca, J. Vondrák, O. Čech, M. Sedlaříková, Supercapacitors: Properties and applications, Journal of Energy Storage, 17(2018) 224-7.

[2] S.P.S. Badwal, S.S. Giddey, C. Munnings, A.I. Bhatt, A.F. Hollenkamp, Emerging electrochemical energy conversion and storage technologies, Frontiers in chemistry, 2(2014) 79.

[3] M. Rapisarda, F. Marken, M. Meo, Graphene oxide and starch gel as a hybrid binder for environmentally friendly high-performance supercapacitors, Communications Chemistry, 4(2021) 169.

[4] E. Faggioli, P. Rena, V. Danel, X. Andrieu, R. Mallant, H. Kahlen, Supercapacitors for the energy management of electric vehicles, Journal of Power Sources, 84(1999) 261-9.

[5] L. Kouchachvili, W. Yaïci, E. Entchev, Hybrid battery/supercapacitor energy storage system for the electric vehicles, Journal of Power Sources, 374(2018) 237-48.

[6] G. de Souza Augusto, J. Scarmínio, P.R. Catarini Silva, A. de Siervo, C.S. Rout, F. Rouxinol, et al., Flexible metal-free supercapacitors based on multilayer graphene electrodes, Electrochimica Acta, 285(2018) 241-53.

[7] C. Lekakou, O. Moudam, F. Markoulidis, T. Andrews, J. Watts, G.J.J.o.N. Reed, Carbon-based fibrous EDLC capacitors and supercapacitors, 2011(2011).

[8] S.G. Kandalkar, D.S. Dhawale, C.-K. Kim, C.D. Lokhande, Chemical synthesis of cobalt oxide thin film electrode for supercapacitor application, Synthetic Metals, 160(2010) 1299-302.

[9] J. Chmiola, C. Largeot, P.L. Taberna, P. Simon, Y. Gogotsi, Monolithic carbide-derived carbon films for micro-supercapacitors, Science (New York, NY), 328(2010) 480-3.

[10] P. Simon, Y. Gogotsi, Materials for electrochemical capacitors, Nanoscience technology: a collection of reviews from Nature journals, (2010) 320-9.

[11] S. Palchoudhury, K. Ramasamy, R.K. Gupta, A. Gupta, Flexible supercapacitors: a materials perspective, Frontiers in Materials, 5(2019) 83.

[12] P. Xie, W. Yuan, X. Liu, Y. Peng, Y. Yin, Y. Li, et al., Advanced carbon nanomaterials for state-of-the-art flexible supercapacitors, Energy Storage Materials, 36(2021) 56-76.

[13] A. Khosrozadeh, M.A. Darabi, M. Xing, Q.J.A.a.m. Wang, interfaces, Flexible electrode design: fabrication of freestanding polyaniline-based composite films for high-performance supercapacitors, 8(2016) 11379-89.

[14] L. Yu, L. Hu, B. Anasori, Y.-T. Liu, Q. Zhu, P. Zhang, et al., MXene-bonded activated carbon as a flexible electrode for high-performance supercapacitors, ACS Energy Letters, 3(2018) 1597-603.

[15] S. Wang, N. Liu, J. Su, L. Li, F. Long, Z. Zou, et al., Highly stretchable and self-healable supercapacitor with reduced graphene oxide based fiber springs, Acs Nano, 11(2017) 2066-74.

[16] S. Ban, K. Malek, C. Huang, Z. Liu, A molecular model for carbon black primary particles with internal nanoporosity, Carbon, 49(2011) 3362-70.

[17] T.A. Silva, F.C. Moraes, B.C. Janegitz, O.J.J.o.N. Fatibello-Filho, Electrochemical biosensors based on nanostructured carbon black: A review, 2017(2017).

[18] K.P. Delgado, P.A. Raymundo-Pereira, A.M. Campos, O.N. Oliveira Jr., B.C. Janegitz, Ultralow Cost Electrochemical Sensor Made of Potato Starch and Carbon Black Nanoballs to Detect Tetracycline in Waters and Milk, 30(2018) 2153-9.

[19] C. Phillips, A. Al-Ahmadi, S.-J. Potts, T. Claypole, D. Deganello, The effect of graphite and carbon black ratios on conductive ink performance, Journal of materials science, 52(2017) 9520-30.

[20] D.M.E.a. Garcia, A.S.T.M. Pereira, A.n.C. Almeida, U.S. Roma, A.B.A. Soler, P.D. Lacharmoise, et al., Large-Area Paper Batteries with Ag and Zn/Ag Screen-Printed Electrodes, 4(2019) 16781-8.

[21] D. Pech, M. Brunet, P.-L. Taberna, P. Simon, N. Fabre, F. Mesnilgrente, et al., Elaboration of a microstructured inkjet-printed carbon electrochemical capacitor, Journal of Power Sources, 195(2010) 1266-9.

[22] F.J. Rodríguez, M.J. Galotto, A. Guarda, J.E. Bruna, Modification of cellulose acetate films using nanofillers based on organoclays, Journal of Food Engineering, 110(2012) 262-8.

[23] M.A. Wsoo, S. Shahir, S.P.M. Bohari, N.H.M. Nayan, S.I. Abd Razak, A review on the properties of electrospun cellulose acetate and its application in drug delivery systems: A new perspective, Carbohydrate research, 491(2020) 107978.

[24] Y. Xu, Q. Hao, D. Mandler, Electrochemical detection of dopamine by a calixarene-cellulose acetate mixed Langmuir-Blodgett monolayer, Analytica chimica acta, 1042(2018) 29-36.

[25] I.A. de Araujo Andreotti, L.O. Orzari, J.R. Camargo, R.C. Faria, L.H. Marcolino-Junior, M.F. Bergamini, et al., Disposable and flexible electrochemical sensor made by recyclable material and low cost conductive ink, 840(2019) 109-16.

[26] T. Kondo, H. Sakamoto, T. Kato, M. Horitani, I. Shitanda, M. Itagaki, et al., Screen-printed diamond electrode: A disposable sensitive electrochemical electrode, Electrochemistry communications, 13(2011) 1546-9.

[27] R.O. Kadara, N. Jenkinson, C.E. Banks, Characterization and fabrication of disposable screen printed microelectrodes, Electrochemistry Communications, 11(2009) 1377-80.

[28] D.S. Rocha, L.C. Duarte, H.A. Silva-Neto, C.L.S. Chagas, M.H.P. Santana, N.R. Antoniosi Filho, et al., Sandpaper-based electrochemical devices assembled on a reusable 3D-printed holder to detect date rape drug in beverages, Talanta, 232(2021) 122408.

[29] H. Li, W. Wang, Q. Lv, G. Xi, H. Bai, Q. Zhang, Disposable paper-based electrochemical sensor based on stacked gold nanoparticles supported carbon nanotubes for the determination of bisphenol A, Electrochemistry Communications, 68(2016) 104-7.

[30] J.R. Camargo, I.A.A. Andreotti, C. Kalinke, J.M. Henrique, J.A. Bonacin, B.C. Janegitz, Waterproof paper as a new substrate to construct a disposable sensor for the electrochemical determination of paracetamol and melatonin, Talanta, 208(2020) 120458.

[31] L.O. Orzari, I.A. de Araujo Andreotti, M.F. Bergamini, L.H.M. Junior, B.C. Janegitz, Disposable electrode obtained by pencil drawing on corrugated fiberboard substrate, Sensors and Actuators B: Chemical, 264(2018) 20-6.

[32] J.H.S. Carvalho, J.L. Gogola, M.F. Bergamini, L.H. Marcolino-Junior, B.C. Janegitz, Disposable and low-cost lab-made screen-printed electrodes for voltammetric determination of L-dopa, Sensors and Actuators Reports, 3(2021) 100056.

[33] B. Liu, H. Shioyama, H. Jiang, X. Zhang, Q. Xu, Metal-organic framework (MOF) as a template for syntheses of nanoporous carbons as electrode materials for supercapacitor, Carbon, 48(2010) 456-63.

[34] I. Danaee, M. Jafarian, F. Forouzandeh, F. Gobal, M.G. Mahjani, Electrochemical impedance studies of methanol oxidation on GC/Ni and GC/NiCu electrode, International Journal of Hydrogen Energy, 34(2009) 859-69.

[35] A. Krause, P. Kossyrev, M. Oljaca, S. Passerini, M. Winter, A. Balducci, Electrochemical double layer capacitor and lithium-ion capacitor based on carbon black, Journal of Power Sources, 196(2011) 8836-42.

[36] X. Ma, X. Song, Z. Yu, S. Li, X. Wang, L. Zhao, et al., S-doping coupled with pore-structure modulation to conducting carbon black: Toward high mass loading electrical double-layer capacitor, Carbon, 149(2019) 646-54.

[37] M.E. Orazem, B. Tribollet, Electrochemical impedance spectroscopy, New Jersey, (2008) 383-9.

[38] A. Lasia, Electrochemical impedance spectroscopy and its applications,  Modern aspects of electrochemistry, Springer2002, pp. 143-248.

[39] M. Nasibi, M.A. Golozar, G. Rashed, Nano zirconium oxide/carbon black as a new electrode material for electrochemical double layer capacitors, Journal of Power Sources, 206(2012) 108-10.

[40] J. Bobacka, A. Lewenstam, A. Ivaska, Electrochemical impedance spectroscopy of oxidized poly (3, 4-ethylenedioxythiophene) film electrodes in aqueous solutions, Journal of Electroanalytical Chemistry, 489(2000) 17-27.

[41] C. Zhang, Y. Xie, J. Wang, A. Pentecost, D. Long, L. Ling, et al., Effect of graphitic structure on electrochemical ion intercalation into positive and negative electrodes, Journal of Solid State Electrochemistry, 18(2014) 2673-82.

[42] J.B. Mitchell, Understanding the Role of Structural Water for High Power Electrochemical Energy Storage in Tungsten Oxide Hydrates: North Carolina State University; 2021.

[43] K.P.D. Orellana, Low Cost, Carbon-Based Micro-and Nano-Structured Electrodes for High Performance Supercapacitors, (2016).

[44] F. Thissandier, A. Le Comte, O. Crosnier, P. Gentile, G. Bidan, E. Hadji, et al., Highly doped silicon nanowires based electrodes for micro-electrochemical capacitor applications, Electrochemistry Communications, 25(2012) 109-11.

[45] Y. Zou, Z. Zhang, W. Zhong, W. Yang, Hydrothermal direct synthesis of polyaniline, graphene/polyaniline and N-doped graphene/polyaniline hydrogels for high performance flexible supercapacitors, Journal of Materials Chemistry A, 6(2018) 9245-56.

[46] J. Zhou, T. Zhu, W. Xing, Z. Li, H. Shen, S. Zhuo, Activated polyaniline-based carbon nanoparticles for high performance supercapacitors, Electrochimica Acta, 160(2015) 152-9.

[47] G. de Souza Augusto, J. Scarmínio, P.R.C. Silva, A. de Siervo, C.S. Rout, F. Rouxinol, et al., Flexible metal-free supercapacitors based on multilayer graphene electrodes, Electrochimica Acta, 285(2018) 241-53.

[48] E. Eustache, R. Frappier, R.L. Porto, S. Bouhtiyya, J.-F. Pierson, T. Brousse, Asymmetric electrochemical capacitor microdevice designed with vanadium nitride and nickel oxide thin film electrodes, Electrochemistry communications, 28(2013) 104-6.

[49] J. Lee, Y.A. Lee, C.-Y. Yoo, J.J. Yoo, R. Gwak, W.K. Cho, et al., Self-templated synthesis of interconnected porous carbon nanosheets with controllable pore size: Mechanism and electrochemical capacitor application, 261(2018) 119-25.