Supplementary material

Eco-Friendly Screen-Printed Sensor Using Tapioca-Based Conductive Ink Modified with Coconut Fibers

Rafaela C. de Freitas a, Jéssica Rocha Camargo a, Laís Canniatti Brazaca b, Lucio Angnes c, Orlando Fatibello-Filho d, Bruno C. Janegitz a*

a Laboratório de Sensores, Nanomedicina e Materiais Nanoestruturados, Federal University of São Carlos, Araras, SP, Brazil

b São Carlos Institute of Chemistry, University of São Paulo, São Carlos, SP 13566-590, Brazil

c Departamento de Química Fundamental, Instituto de Química, Universidade de São Paulo, Av. Prof. Lineu Prestes, 748 – 05508-000, São Paulo, SP, Brazil

d Laboratório de Analítica, Bioanalítica, Biosensores, Electroanalítica e Sensores, Departamento de Química, Universidade Federal de São Carlos (UFSCar), CP 676, 13560-970 São Carlos-SP, Brazil

*Corresponding authors: Bruno C. Janegitz, brunocj@usfscar.br and Jéssica Rocha Camargo, jessica.10.camargo@gmail.com

Figure S1. (A) SPE fabricated using a 44-mesh screen and a water-based conductive ink composed of tapioca and carbon materials. (B) Electrode dimensions compared to a ruler for scale.

Figure S2. Cyclic voltammograms obtained with SPE conductive ink based on 6% (w/v) tapioca dispersion with 1% (w/w) of glycerol (pink line) and sorbitol (red line), both with 40% (w/w) GR for a 1.0 mmol L−1 [Fe(CN)6]3−/4− in 0.1 mol L−1 KCl solution, v = 50 mV s−1

Figure S3. Cyclic voltammograms obtained with SPE conductive ink based on a 6% (w/v) tapioca dispersion with 1% (w/w) sorbitol and 40% (w/w) GR in different drying times, 12 h (black line), 24 h (red line) and 48 h (blue line) for a 1.0 mmol L1 [Fe(CN)6]3−/4− in 0.1 mol L1 KCl solution, v = 50 mV s1

Figure S4. Cyclic Voltammograms obtained with SPE conductive ink based on a 6% (w/v) tapioca dispersion with 1% (w/w) sorbitol and 40% (w/w) GR for a 1.0 mmol L1 [Fe(CN)6]3/4 in 0.1 mol L1 KCl solution, v = 50 mV s1 with deposition of 1 (blue line) and 2 layers (pink line)

Figure S5. (A) CVs were obtained with screen-printed sensors based on conductive inks using dispersion of 6%(w/v) TP and 1% (w/w) sorbitol, varying compositions the carbon material in 42,5% GR/ 2,5% CB (green line), 40% GR/ 5% CB (blue line), 35% GR/ 10% CB (red line) for a 1.0 mmol L−1 [Fe(CN)6]3−/4 in 0.1 mol L−1 KCl solution, v = 50 mV s−1. (B) Cyclic voltammograms obtained with screen-printed sensors based in conductive inks with 35% GR/ 10% CB, varying concentrations of TP in dispersions in 3% (w/V) TP (black line) and 4% (w/V) TP (red line) and 1% (w/w) sorbitol in both, for 1.0 mmol L−1 [Fe(CN)6]3−/4− in 0.1 mol L−1 KCl solution, v = 50 mV s−1.

Figure S6. (A) Cyclic voltammograms obtained with Gr-CB-S-TP/acetate sensor for 1.0 mmol L−1 [Fe(CN)6]3−/4 in 0.1 mol L−1 KCl solution, v = 50 mV s−1. (B) Dependence of current with different electrode thermal treatments for 1 h in an oven.

Figure S7. (A) Cyclic voltammograms obtained with Gr-CB-S-TP/acetate sensor with two different reference electrodes, carbon pseudo-reference (red line) and silver pseudo-reference (blue line) for 1.0 mmol L−1 [Fe(CN)6]3−/4 in 0.1 mol L−1 KCl solution, v = 50 mV s−1.

Figure S8. (A) Nyquist diagram obtained by Gr-CB-TP/acetate sensor in the presence of 1.0 mmol L⁻¹ [Fe(CN)₆]³⁻/⁴⁻ and 0.1 mol L⁻¹ KCl; E1/2 = 0.05 V, equivalent circuit inserted: [R(RC)(RC)(RC)]. (B) Nyquist diagram obtained by CF-Gr-CB-TP/acetate sensor in the presence of 1.0 mmol L⁻¹ [Fe(CN)₆]³⁻/⁴⁻ and 0.1 mol L⁻¹ KCl; E1/2 = 0.05 V, equivalent circuit inserted: [R(RC)(RC)(RC)]

Figure S9. (A) Nyquist diagram obtained by Gr-CB-TP/acetate sensor in the presence of 1.0 mmol L⁻¹ [Fe(CN)₆]³⁻/⁴⁻ and 0.1 mol L⁻¹ KCl; E1/2 = 0.05 V, equivalent circuit inserted: [R(RC)(RC)(RC)], n = 5.

Figure S10. DP voltammograms (red line) and SW voltammograms (blue line) obtained with Gr-CB-S-TP/acetate sensor for 100 mol L1 uric acid in 0.2 mol L1 PBS solution (pH = 7.0); SWV, s = 2 mV, a = 20 mV and f = 20 Hz; DPV s = 10 mV, a = 25 mV, t = 50 ms

Figure S11. (A) Cyclic voltammograms obtained with CF-Gr-CB-S-TP/acetate sensor varying CF from 2% to 4% for 0.01 mol L−1 H2O2 in 0.2 mol L−1 PBS solution (pH = 7.4), v = 25 mV s−1

Figure S12. CV were obtained with the biosensor with 2% (m/m) CF (pink line) and with SPE new layer of conductive ink (blue line), in the presence for 0.01 to 1.0 mol L1 H2O2 in 0.2 mol L1 PBS solution (pH = 7.4), v = 25 mV s1

Figure S13. (A) Chronoamperometry using the CF-Gr-CB-S-TP/acetate sensor with 2% CF in the absence (black line) and the presence of 1.0 and 10 mmol L−1 H₂O₂ (blue line and red line) solution prepared in 0.2 mol L⁻¹ PBS (pH 7.4)

Table S1. Interference study for uric acid and H2O2 detection in the presence of ascorbic acid, catechol, dopamine and urea in the same concentration of 50 μmol L−1.

| Interferers (1:1 proportion) | Percentage (%) |
| --- | --- |
| Uric acid electrochemical sensor |  |
| Ascorbic acid | −15.6 |
| Catechol | −7.82 |
| Dopamine | −11.5 |
| Urea | −9.58 |
| H2O2 electrochemical sensor |  |
| Ascorbic acid | 32.2 |
| Catechol | −16.6 |
| Dopamine | −30.9 |
| Urea | −8.24 |

Table s2. Comparison with other devices in the literature for uric acid and H2O2

|  | Sensors | Detection | Electrochemical technique | Linear range μmol L−1 | LOD | Literature |
| --- | --- | --- | --- | --- | --- | --- |
| Uric Acid | Uricase/Chi-Gr cry/PB/SPCE 1 | Oxidation | Amperometry | 2.5 – 400 μmol L−1 | 2.5 μmol L−1 | [1] |
|  | rGO-SPCE 2 | Oxidation | DPV | 10 - 3000 μmol L−1 | 0.35 μmol L−1 | [2] |
|  | Poly(4- ASA)-PB-SPE 3 | Oxidation | Amperometry | 10 - 200 μmol L−1 | 3.0 μmol L−1 | [3] |
|  | MWCNT-SPE 4 | Oxidation | LSV | 1.0 – 100 μmol L−1 | 0.86 μmol L−1 | [4] |
|  | Gr-CB-S-TP/acetate | Oxidation | DPV | 5.0 – 100 μmol L−1 | 0.34 μmol L−1 | This work |
| H2O2 | AuSPE electrode 5 | Oxidation | Amperometry | 10 - 1000 μmol L−1 | 0.37 μmol L−1 | [5] |
|  | Pt/PPy/GC electrode 6 | Reduction | Amperometry | 1.0 – 8.0 mmol L−1 | 1,2 μmol L−1 | [6] |
|  | HRP/Au/ERGO-CHIT/GCE electrode 7 | Reduction | Amperometry | 0.01 - 6.31 mmol L−1 | 4,0 μmol L−1 | [7] |
|  | Nf/Pd@Ag/rGO-NH2/GC electrode 8 | Reduction | Amperometry | 0.002 - 19.5 mmol L−1 | 0,7 μmol L−1 | [8] |
|  | FC-GR-CB-S-TP/Acetate | Oxidation | CV | 2.3 - 11.4 mmol L−1 | 0,6 mmol L−1 | This work |

1 biosensor from SPE modified with Prussian blue and graphene and chitosan cryogel composite; 2 Screen-printed carbon electrode (SPCE) chemically modified with reduced graphene oxide (rGO); 3 SPE modified with Prussian blue/poly(4-aminosalicylic acid) and uricase; 4 SPE modified with multi-walled carbon nanotubes (MWCNT); 5 SPE modified with gold porous; 6 electrochemical biosensor with hybrids polypyrrole/Pt microspheres; 7 electrochemical biosensor with horseradish peroxidase immobilized in graphene oxide, chitosan and gold nanocomposite; 8 GCE modified with reduced graphene oxide functionalized and Pd@Ag bimetallic nanoparticles;

Figure S14. AGREE score for the CF-Gr-CB-S-TP/acetate sensor

References:

[1] R. Jirakunakorn, S. Khumngern, J. Choosang, P. Thavarungkul, P. Kanatharana, A. Numnuam, Uric acid enzyme biosensor based on a screen-printed electrode coated with Prussian blue and modified with chitosan-graphene composite cryogel, Microchemical Journal 154 (2020) 104624.https://doi.org/10.1016/j.microc.2020.104624

[2] P. Kanyong, S. Rawlinson, J. Davis, A voltammetric sensor based on chemically reduced graphene oxide-modified screen-printed carbon electrode for the simultaneous analysis of uric acid, ascorbic acid and dopamine, Chemosensors 4(4) (2016) 25.https://doi.org/10.3390/chemosensors4040025

[3] F.S. da Cruz, F. de Souza Paula, D.L. Franco, W.T.P. dos Santos, L.F. Ferreira, Electrochemical detection of uric acid using graphite screen-printed electrodes modified with Prussian blue/poly (4-aminosalicylic acid)/Uricase, Journal of Electroanalytical Chemistry 806 (2017) 172-179.https://doi.org/10.1016/j.jelechem.2017.10.070

[4] P. Fanjul‐Bolado, D.H. Santos, V.M. Montoya, A. Costa‐García, Uric Acid Determination by Adsorptive Stripping Voltammetry on Multiwall Carbon Nanotubes Based Screen‐Printed Electrodes, Electroanalysis 27(5) (2015) 1276-1281.https://doi.org/10.1002/elan.201400690

[5] C. Maksuk, C. Tinala, W. Somboot, J. Jakmunee, F. Marken, T. Kanyanee, Rapid Determination of Hydrogen Peroxide in Milk with Non‐enzymatic Amperometric Sensor Based on Porous Gold Modified Screen‐printed Electrode in Online Dialysis System, Electroanalysis 35(2) (2023) e202100691.https://doi.org/10.1002/elan.202100691

[6] X. Bian, X. Lu, E. Jin, L. Kong, W. Zhang, C. Wang, Fabrication of Pt/polypyrrole hybrid hollow microspheres and their application in electrochemical biosensing towards hydrogen peroxide, Talanta 81(3) (2010) 813-818.https://doi.org/10.1016/j.talanta.2010.01.020

[7] M. Devaraj, S. Rajendran, J.N. Jebaranjitham, D. Ranjithkumar, M. Sathiyaraj, J. Manokaran, E. Sundaravadivel, J. Santhanalakshmi, L.C. Ponce, Horseradish peroxidase-immobilized graphene oxide-chitosan gold nanocomposites as highly sensitive electrochemical biosensor for detection of hydrogen peroxide, Journal of the Electrochemical Society 167(14) (2020) 147517.https://doi.org/10.1149/1945-7111/abc35e

[8] M. Guler, V. Turkoglu, A. Bulut, M. Zahmakiran, Electrochemical sensing of hydrogen peroxide using Pd@ Ag bimetallic nanoparticles decorated functionalized reduced graphene oxide, Electrochimica Acta 263 (2018) 118-126.https://doi.org/10.1016/j.electacta.2018.01.048