Table 1. Comparison of the analytical characteristics obtained with PB/CB-PLA for the detection of hydrogen peroxide with works reported in the literature.

| Electrode | Analyte | Linear Range (µmol L-1) | LOD (µmol L-1) | Ref. |
| --- | --- | --- | --- | --- |
| GOx-modified 3D-printed biosensora | H2O2 | 50.0 – 500.0 | 2.97 | [50] |
| 3D pyrolytic carbon microelectrodes | H2O2 | 0.3 – 8.0 | 0.16 | [51] |
| PB/G/PLAb | H2O2 | 1.0 – 700.0 | 0.56 | [52] |
| 3DGrE/PBc | H2O2 | 1.0 – 700.0 | 0.11 | [53] |
| DMF-EC/HRPd | H2O2 | 0 – 100.0 and 150.0 – 600.0 | 11.10 | [54] |
| DMF-EC/AuNPs/HRPe | H2O2 | 0 – 100.0 and 150.0 – 600.0 | 9.10 | [54] |
| 3D e-wellsf | H2O2 | 1500.0 – 13500.0 | n.mh | [55] |
| CB/PLA and GR/PLAg | H2O2 | 500.0 – 15000.0 | n.mh | [56] |
| PB/CB-PLA | H2O2 | 5.0 – 350.0 | 1.03 | This work |

a3D-printed nanocarbon glucose oxidase-based biosensor; bPrussian blue films on additive manufactured electrodes from iron impurities found at the graphene-polylactic acid; c3D printed graphene electrode with Prussian blue. d3D-printed graphene-PLA electrode after chemical and electrochemical treatments modified with horseradish peroxidase. e3D-printed graphene-PLA electrode after chemical and electrochemical treatments modified with gold nanoparticles plus horseradish peroxidase. f3D-printed electrochemical microtitration wells. gCarbon black/PLA and graphene/PLA. hnot mentioned.

Table 2. Comparison of the manufacturing characteristics of CB-PLA with lab-made composite materials for electroanalysis of works reported in the literature.

| Thermoplastic | Conductive material | Composite preparation | Manufacturing time / h | Proposed application | Ref. |
| --- | --- | --- | --- | --- | --- |
| PLA | graphene | Dissolution in xylene | 6.0 + solvent evaporation | Anode for batteries | [11] |
| PLA | 2D-MoSe2 | Dissolution in xylene | 6.0 + solvent evaporation | Anode and cathode for WS | [57] |
| PLA | graphite | Dissolution in chloroform | 96.2 | Detection of Pb2+ and Cd2+ | [58] |
| ABS | graphite | Dissolution in acetone | 72.2 | Detection of PAR | [59] |
| G-PLA | Ni(OH)2 | Dissolution in acetone/chloroform | - | Detection of glucose | [17] |
| PLA | NG | Dissolution in xylene | 6.0 + solvent evaporation | Detection of Pb2+ and Cd2+ | [18] |
| PLA | graphite | Dissolution in acetone/chloroform | 15.5 | Detection of UA, DA, and SARS-CoV-2 | [13] |
| PLA | carbon black | Dissolution in acetone/chloroform | 15.2 | Detection of CA, HQ, and H2O2 | This work |

DA: dopamine; NG: nanographite; PAR: paracetamol; UA: uric acid; WS: water splitting;

Table S1. Comparison between the calculated electroactive areas (Aelect.) for 3D printed electrodes using the Randles-Ševčíck equation for quasi-reversible processes, with the respective geometrical area values (Ageom.) and the ratio values (Aratio), corresponding to Aelect. divided by the Ageom.(n = 3).

| Electrode | Electroactive area / mm2 | Geometrical area / mm2 | Aratio |
| --- | --- | --- | --- |
| CB-PLA | 21.1 ± 0.1 | 12.6 | 1.7 ± 0.1 |
| CB-PLA treated | 26.8 ± 0.1 | 12.6 | 2.1 ± 0.1 |
| Proto-pasta | 19.1 ± 0.1 | 12.6 | 1.5 ± 0.1 |
| Proto-pasta treated | 20.4 ± 0.3 | 12.6 | 1.6 ± 0.1 |

Table S2. Determination of catechol in tap water samples (n = 3).

|  | Spiked (µmol L-1) | Found (µmol L-1) | Recovery (%) |
| --- | --- | --- | --- |
| Sample 1 | 5.00 | 5.09 ± 0.1 | 102 ± 2. |
|  | 10.0 | 10.7 ± 0.1 | 107 ± 1 |
|  | 50.0 | 49.5 ± 0.4 | 99.0 ± 0.7 |
| Sample 2 | 5.00 | 5.06 ± 0.1 | 101 ± 2 |
|  | 10.0 | 10.7 ± 0.2 | 107 ± 3 |
|  | 50.0 | 50.8 ± 0.6 | 102 ± 1 |

Table S3. Determination of hydroquinone in tap water samples (n = 3).

|  | Spiked (µmol L-1) | Found (µmol L-1) | Recovery (%) |
| --- | --- | --- | --- |
| Sample 1 | 5.00 | 4.98 ± 0.5 | 99.7 ± 9.7 |
|  | 10.0 | 10.8 ± 0.5 | 107 ± 5.0 |
|  | 30.0 | 32.6 ± 0.6 | 109 ± 2.1 |
| Sample 2 | 5.00 | 4.55 ± 0.3 | 91.1 ± 6.5 |
|  | 10.0 | 11.2 ± 0.7 | 112 ± 6.7 |
|  | 30.0 | 29.7 ± 1.2 | 99.0 ± 4.0 |

Table S4. Comparison of the analytical characteristics obtained with CB-PLA for the detection of CA and HQ with works reported in the literature.

| Electrode | Analyte | Linear Range (µmol L-1) | LOD (µmol L-1) | Ref. |
| --- | --- | --- | --- | --- |
| Tyr-DHP/rGO-PLAa | CA | 30.0 – 700.0 | 0.26 | [1] |
| 3D printed flow cellb | CA | 5.1 – 103.0 | 1.4 | [2] |
| Mg–ZnO/MCPEc | CA | 10.0–100.0 | 0.69 | [3] |
| GE/β-CD-AuNPs/Tyrd | CA | 1.56- 25.0 | 0.42 | [4] |
| CB-PLA | CA | 0.5 – 60.0 | 0.02 | This work |
| Biosensore | HQ | 2.5 – 1450.0 | 0.5 | [5] |
| - G-PBAT-sensorf | HQ | 100.0 – 1400.0 | 1.01 | [6] |
| GCE/Zn@ZnOg | HQ | 10.0 – 90.0 | 0.1 | [7] |
| GCE/CAU-1h | HQ | 0.5 – 1500.0 | 0.07 | [8] |
| CB-PLA | HQ | 1.0 – 50.0 | 0.22 | This work |

atyrosinase-based biosensor; belectrochemical flow cells with embedded carbon-composite electrodes in a single step using simultaneous 3D printing of insulating poly(lactic acid) and a commercially available graphene–PLA composite; cβ-cyclodextrin-capped gold nanoparticles on graphite electrode surface and dMg-doped ZnO modified carbon paste electrode; ethreedimensional architecture of Prussian blue nanoparticles (PBNPs)/ Pt nanoparticles (PtNPs) composite film; fgraphite and the polymer poly (butylene adipate-co-terephthalate) sensor; gglassy carbon electrode modified with zinc@zinc oxide; hAl-MOF fabricated glassy carbon electrode.

Table S5. Determination of hydrogen peroxide in tap milk samples (n = 3).

|  | Spiked (µmol L-1) | Found (µmol L-1) | Recovery (%) |
| --- | --- | --- | --- |
| Milk sample | 5.00 | 4.40 ± 0.1 | 88.0 ± 2.3 |
|  | 10.0 | 9.40 ± 0.7 | 94.0 ± 7.4 |
|  | 50.0 | 48.5 ± 2.6 | 97.0 ± 5.4 |
|  | 150 | 135 ± 9.9 | 89.7 ± 7.4 |
|  | 250 | 213 ± 15 | 85.2 ± 7.0 |