Table 1. Comparison of works in the literature for the determination of 3-NLT

| Device |  | Linear range mol L) |  | LOD  mol L) | Ref. |
| --- | --- | --- | --- | --- | --- |
| Paper-SPE | 0.50 – 1000.0 |  | 0.05 |  | [29] |
| Paper-bioSPE | 0.50 – 1000.0 |  | 0.02 |  | [57] |
| AuNPs/MIP/AMWCNT@GONRs/GCE | 0.20 – 50.0 |  | 0.05 |  | [67] |
| CdWO4/ND@RGO/SPE | 0.01 – 1840.0 |  | 0.001 |  | [23] |
| CNTs-GV/PET (PBS) | 0.70 – 100.0 |  | 0.53 |  | This work This work |
| CNTs-GV/PET (Human Serum) | 3.0 – 100.0 |  | 1.35 |  |  |

Paper-SPE: paper-based sensor printed with commercial conductive ink based on carbon and silver on waterproof paper containing beeswax; Paper-bioSPE: paper-based sensor printed with commercial conductive ink based on carbon and silver on waterproof paper containing beeswax, modified with phenol monomer; AuNPs/MIP/AMWCNT@GONRs/GCE: electropolymerized sensor with molecularly printed polypyrrole modified with multi-walled CNTs and graphene; CdWO4/ND@RGO/SPE: CdWO4 Nanodots decorated with reduced graphene oxide in a commercial screen-printed sensor;

Table S1. Approximate value of sensor preparation components

| Components | Market value (US$) | Value for production of 2.3 g of ink |
| --- | --- | --- |
| Glass Varnish (ACRILEX®) 100 mL | 5.60 | 0.11 (2 g) |
| Carbon nanotubes 200g | 483.00 | 0.7243 (0.3 g) |
| Adhesive paper (m2) | 0,20 | 0.008 (0.04 m2) |
| PET | - | - |
| Total | - | 0.8423/30 units | 0.03/unit |

Table S2. Composition of synthetic urine sample.

| Reagent | Concentration (g L) |
| --- | --- |
| CaCl2.2H2O | 1.13 |
| Urea | 25.0 |
| NaH2PO4 | 1.40 |
| NaCl | 2.92 |
| Na2SO4 | 2.25 |
| KCl | 1.60 |
| NH4Cl | 1.00 |
| Creatinine | 1.10 |

Table S3. Optimization of SWV parameters and working pH value of a 0.1 mol L PBS solution, for 3-NLT detection.

| Parameter | Range | Optimum value |
| --- | --- | --- |
| Frequency | 10 - 80 Hz | 60 Hz |
| Amplitude | 20 - 90 mV | 70 mV |
| Step | 1 - 8 mV | 7 mV |
| pH | 6.0 - 7.5 | 7.5 |

Table S4. Concentrations of 3-NLT and recovery values obtained in synthetic urine samples using CNTs-GV/PET electrodes, with the respective standard deviation values (n = 3).

| Sample | Added (mol L) | Found (mol L) | Recovery (%) |
| --- | --- | --- | --- |
| A1 | 1.0 | 1.0 | 101 ± 6 |
| A2 | 10.0 | 10.6 | 106 ± 13 |
| A3 | 30.0 | 28.6 | 95 ± 6 |