Tables

Table 1. Analytical performance obtained for the determination of L-cysteine using different electrodes.

| Electrode | Supporting electrolyte | Technique | LDR (μmol L-1) | Sensitivitya (AL cm-2 mol-1) | LOD (μmol L-1) | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| GCE/RGO | PB pH 7.4 | Amperometry | 5.0–47 | 0.211 | − | [42] |
| MWCNT–PVP | PBS pH 7.0 | Amperometry | 5.0−60 | 0.100 | 1.50 | [43] |
| FTO/AuNP/MnP | BRB pH 7.0 | CA | 12.2–33.6 | 0.027 | 2.40 | [44] |
| SPE/PB | ABS pH 6.0 | CA | 100–600 | − | 67.4 | [27] |
| SPE/PB-A | ABS pH 6.0 | CA | 300–800 | − | 149 |  |
| BDDP | PB pH 7.0 | CV | 1.0–194 | 0.226 | 0.620 | [45] |
| CuFe2O4/rGO-Au | PBS pH 6.5 | CV | 50–400 | 0.100 | 0.383 | [46] |
| BDD-Mo(IV) | BBS pH 10 | CV | 0.0−500 | − | 0.3 | [47] |
| GCE-CTC | PBS pH 7.0 | CV | 0.0−40 | 0.320 | 0.6 | [48] |
| QMCPE | PB pH 7.0 | DPV | 1.0−1,000 | − | 0.22 | [49] |
| GCE-Au | PBS pH 7.5 | DPV | 0.22–50 | − | 0.074 | [50] |
| PLA-GDMF-EC+PB | PBS pH 7.4 | Amperometry | 3.0−230 | 0.167 | 0.858 | This work |

a Calculated by the geometric area (cm2) of the electrodes. CA: Chronoamperometry; CV: Cyclic voltammetry; DPV: Differential pulse voltammetry. SPE/PB: Screen-printed electrode modified with Prussian blue; SPE/PB-A: Screen-printed electrode modified with Prussian blue analog; GCE/RGO: Glassy carbon electrode modified with reduced graphene oxide and iron porphyrin; MWCNT–PVP: Electrode modified with poly-4-vinylpyridine and copper complex in carbon nanotubes; FTO/AuNP/MnP: Glass electrode with fluorine oxide and tin modified with gold nanoparticles and manganese porphyrin; BDDP: Boron-doped diamond screen-printed electrode; CuFe2O4/rGO-Au: Electrode modified with CuFe2O4 and reduced graphene oxide decorated with gold nanoparticles; BDD-Mo(IV): Octacyanomolybdate(IV) complex at boron doped diamond electrode; GCE-CTC: Glassy carbon electrode modified with cyclotricatechylene; QMCPE: Carbon paste electrode modified with quinizarine; GCE-Au: Glassy carbon electrode modified with gold nanoparticles.

Table 2. Detection of L-cysteine in spiked human serum samples (n = 3).

| L-cysteine concentration (µmol L−1) |  | Recovery (%) |
| --- | --- | --- |
| Spiked | Recovered |  |
| 10.0 | 9.74±0.53 | 97.4 |
| 100 | 90.9±4.4 | 90.7 |
| 350 | 360±1 | 103 |