Tables

Table 1. Thermogravimetric analysis of the different components and filaments used throughout this work. Highlighting the average onset temperatures, average final masses, and the conductive filler contents where applicable. Uncertainties in the values represent the standard deviation from three separate measurements.

| Sample | Onset Temp 1 (°C) | Onset Temp 2 (°C) | Final Mass (wt%) | Filler Content (wt%) |
| --- | --- | --- | --- | --- |
| Natural PLA | 305 ± 5 | N/A | 3 ± 2 | N/A |
| PES | 198 ± 1 | N/A | 1 ± 1 | N/A |
| Commercial | 304 ± 2 | 436 ± 4 | 24 ± 2 | 21 ± 3 |
| rPLA/CB | 230 ± 4 | N/A | 22 ± 1 | 19 ± 3 |
| rPLA/CB/S-COOH-MWCNT | 219 ± 4 | N/A | 23 ± 1 | 20 ± 3 |
| rPLA/CB/L-COOH-MWCNT | 219 ± 1 | N/A | 23 ± 1 | 20 ± 3 |

Table 2. Comparison of the calculated heterogenous electron rate constant, and electroactive area for AMEs printed using the four filaments before and after activation. Calculated using ferrocenemethanol (1 mM, 0.1 M KCl) and a geometric area of 0.236 cm2.

| AME Filament |  | k0 (× 10-3 cm s-1) | Areal (cm2) | Areal (%) |
| --- | --- | --- | --- | --- |
| Commercial CB | As printed | 0.66 ± 0.10 | 0.64 ± 0.04 | 64 ± 4 |
|  | Activated | 1.19 ± 0.19 | 1.35 ± 0.02 | 135 ± 2 |
| r-PLA 25% CB | As printed | 1.53 ± 0.50 | 1.17 ± 0.04 | 117 ± 4 |
|  | Activated | 1.83 ± 0.44 | 1.76 ± 0.04 | 176 ± 4 |
| r-PLA, 15 % CB 10% S-COOH-MWCNT | As printed | 1.47 ± 0.31 | 0.90 ± 0.02 | 90 ± 2 |
|  | Activated | 1.70 ± 0.35 | 2.04 ± 0.02 | 204 ± 2 |
| r-PLA, 15 % CB 10% L-COOH-MWCNT | As printed | 1.74 ± 0.58 | 0.82 ± 0.04 | 82 ± 4 |
|  | Activated | 1.85 ± 0.42 | 2.11 ± 0.03 | 211 ± 3 |

Table 3. Detection of Yellow Fever virus in spiked human serum.

|  | Added (µM) | Found (µM) | Recovery (%) | RSD (%) |
| --- | --- | --- | --- | --- |
| Human Serum Sample | 1.00 | 1.05 ± 0.12 | 105 | 4.71 |
|  | 5.00 | 5.11 ± 1.06 | 102 | 2.17 |
|  | 10.0 | 9.56 ± 1.95 | 95.6 | 4.38 |