Supplementary Data

Sustainable electrochemical sensor from CO2 laser pyrolyzed green leaves for carbendazim detection

Beatriz F. Germinarea, Jéssica R. Camargoa, Wilson S. Fernandes-Juniora,b, Bruno C. Janegitza,b*

a Laboratory of Sensors, Nanomedicine, and Nanostructured Materials, Federal University of São Carlos, 13604-900, Araras, São Paulo, Brazil

b Center for Sciences and Technology for Sustainability, Federal University of São Carlos, 18052-780, Sorocaba, São Paulo, Brazil

*Corresponding authors: brunocj@ufscar.br (B. C. Janegitz), jessica.10.camargo@gmail.com (J. R. Camargo)

Figure S1. Green leaves waterproofing process in 0.3 mol L-1 sodium citrate: (A) Addition of the sodium citrate solution to the container. (B) Addition of the leaf to the sodium citrate solution. (C) Immersion of the leaf in the sodium citrate solution for 1 minute. (D) Drying of the leaf after 24h

Figure S2. (A) Cyclic voltammograms obtained by CO2P-GLE in the absence and presence of 5.0 mmol L−1 FcMeOH, in 0.1 mol L−1 KCl, varying power from 8.3% (50 W) to 8.5% (50 W). Scan rate: 50 mV s-1. (B) Cyclic voltammograms obtained by CO2P-GLE in the absence and presence of 5.0 mmol L−1 FcMeOH, in 0.1 mol L−1 KCl, varying printing speed from 80 to 110 mm s-1. Scan rate: 50 mV s-1. (C) Cyclic voltammograms obtained by CO2P-GLE in the absence and presence of 5.0 mmol L−1 FcMeOH, in 0.1 mol L−1 KCl, varying laser distance from 11 to 17 mm. Scan rate: 50 mV s-1. (D) Cyclic voltammograms obtained by CO2P-GLE in the absence (dashed line) and presence (solid line) of 5.0 mmol L−1 FcMeOH, in 0.1 mol L−1 KCl, with a scan rate of 50 mV s-1

Table S1. CO2 laser printing operational parameters of the electrochemical system

| Operational Parameters | Tested Parameters | Chosen Parameters |
| --- | --- | --- |
| Power (% - 50 W) | 8.3 - 8.5 | 8.5 |
| Printing speed (mm s−1) | 80 - 110 | 110 |
| Laser distance (mm) | 11 - 17 | 17 |
| Cutting speed (mm s-1) | 10 | 10 |

Figure S3. (A) Cyclic voltammograms obtained by CO2P-GLE in the presence of 5.0 mmol L-1 FcMeOH in 0.1 mol L-1 KCl. Scan rate: 50 mV s-1. (B) Cyclic voltammograms obtained by CO2P-GLE in the presence of 1.0 mmol L-1 potassium ferri-ferrocyanide in 0.1 mol L-1 KCl. Scan rate: 50 mV s-1. (C) Cyclic voltammograms obtained by CO2P-GLE in the presence of 1.0 mmol L-1 hexaammineruthenium in 0.1 mol L-1 KCl. Scan rate: 50 mV s-1

Figure S4. Redox process of FcMeOH, where it loses an electron at the iron center of the ferrocene core, and this loss converts the ferrocene core from Fe (II) to Fe (III), forming ferricenium methanol

Figure S5. Cyclic voltammograms obtained by CO2P-GLE in the absence (dash line) and presence of 1.0 mmol L−1 FcMeOH (blue line) and 5.0 mmol L−1 FcMeOH (green line), in 0.1 mol L−1 KCl. Scan rate: 50 mV s-1

Figure S6. Cyclic voltammograms obtained by CO2P-GLE with (blue line) and without (black line) the waterproofing process in the absence (dash line) and presence (solid line) of 1.0 mmol L−1 CBZ, in 0.1 mol L−1 phosphate buffer (pH 7.0). Scan rate: 50 mV s-1

Figure S7. Differential pulse (black line) and square wave (blue line) voltammograms, with baseline correction, obtained by CO2P-GLE in the presence of 1.0 mmol L−1 CBZ, in 0.1 mol L−1 phosphate buffer (pH 7.0); DPV parameters: pulse amplitude = 10 mV; pulse modulation time = 50 ms; ν = 30 mV s−1. SWV parameters: pulse amplitude = 20 mV; potential step = 5 mV; and frequency = 6 Hz

Figure S8. (A) Square wave voltammograms obtained by CO2P-GLE in the presence of 1.0 mmol L-1 CBZ, in 0.1 mol L-1 phosphate buffer, varying pH from 5.0 to 8.0; SWV parameters: pulse amplitude = 20 mV; potential step = 5 mV; and frequency = 6 Hz. (B) Plot of E vs. pH

Figure S9. Speciation diagram for CBZ

Figure S10. (A) Square wave voltammograms obtained by CO2P-GLE in the presence of 1.0 mmol L−1 CBZ, in 0.1 mol L−1 phosphate buffer (pH 7.0) varying frequency from 5 to 50 Hz. (B) Scatter plot of the correlation I vs. Frequency (Hz). (C) Square wave voltammograms obtained by CO2P-GLE in the presence of 1.0 mmol L−1 CBZ, in 0.1 mol L−1 phosphate buffer (pH 7.0) varying amplitude from 10 to 100 mV. (D) Scatter plot of the correlation I vs. Amplitude (mV). (E) Square wave voltammograms obtained by CO2P-GLE in the presence of 1.0 mmol L−1 CBZ, in 0.1 mol L−1 phosphate buffer (pH 7.0) varying potential step from 1 to 10 mV. (F) Scatter plot of the correlation I vs. Potential step (mV)

Table S2. Operational parameters for SWV technique optimization, in the presence of 1.0 mmol L−1 CBZ, in 0.1 mol L−1 phosphate buffer (pH 7.0)

| Operational Parameters | Tested Parameters SWV | Chosen Parameters SWV |
| --- | --- | --- |
| Frequency (Hz) | 5 - 50 | 5 |
| Pulse amplitude (mV) | 10 - 100 | 90 |
| Potential step (mV) | 1 - 10 | 5 |

Figure S11. (A) Square wave voltammograms obtained by CO2P-GLE in the presence of 10 μmol L-1 CBZ and interfering species found in the real samples in 1:1 (analyte:interferent), such as KCl, CaCl2, CA, AA, and PQ, in 0.1 mol L-1 phosphate buffer; SWV parameters: pulse amplitude = 90 mV; potential step = 5 mV; and frequency = 5 Hz. (B) Evaluation of the selectivity and interference tolerance of the CO2P-GLE sensor for CBZ detection in the presence of common interferents in a ratio of 1:1, including KCl, CaCl₂, citric acid (CA), ascorbic acid (AA), and paraquat (PQ). The red dashed line indicates the current response to CBZ, serving as a reference for comparison

Figure S12. (A) Square wave voltammograms obtained by CO2P-GLE in the presence of 10 μmol L-1 CBZ and interfering species found in the real samples in 1:10 (analyte:interferent), such as KCl, CaCl2, CA, AA, and PQ, in 0.1 mol L-1 phosphate buffer; SWV parameters: pulse amplitude = 90 mV; potential step = 5 mV; and frequency = 5 Hz. (B) Evaluation of the selectivity and interference tolerance of the CO2P-GLE sensor for CBZ detection in the presence of common interferents in a ratio of 1:1, including KCl, CaCl₂, citric acid (CA), ascorbic acid (AA), and paraquat (PQ). The red dashed line indicates the current response to CBZ, serving as a reference for comparison

Figure S13. (A) Square wave voltammograms obtained by CO2P-GLE in the presence of 10 μmol L-1 CBZ, in 0.1 mol L−1 phosphate buffer (pH 7.0), in the same electrode (n = 5). (B) Square wave voltammograms obtained by CO2P-GLE in the presence of 10 μmol L-1 CBZ, in 0.1 mol L−1 phosphate buffer (pH 7.0), in five different electrodes (n = 5); SWV parameters: pulse amplitude = 90 mV; potential step = 5 mV; and frequency = 5 Hz

Figure S14. EDS data of the (A) bare leaf, (B) sodium citrate leaf, and (C) pyrolyzed electrode surface

Figure S15. (A) Thermogravimetric analysis (TGA) of bare leaf (black line), sodium citrate leaf (red line) and pyrolyzed electrode (blue line). (B) Derivative thermogravimetry (DTG) of pyrolyzed electrode (blue line), (C) sodium citrate leaf (red line), and (D) bare leaf (black line)

Figure S16. Cyclic voltammograms obtained by CO2P-GLE in the presence of 5.0 mmol L−1 FcMeOH, in 0.1 mol L-1 KCl, on the fabrication day (black line), 1 day after fabrication (red line), 2 days after fabrication (blue line), 3 days after fabrication (pink line), 4 days after fabrication (green line), and 5 days after fabrication (orange line). Scan rate: 50 mV s-1