Tailoring ultra-flexibility in eco-friendly conductive filaments: the use of polypropylene in the development of a 3d-printed carbon black-based electrochemical sensor

Lucas V. Bertolim a,b, Luiz R. G. Silva c, Jéssica Santos Stefano c,d, Bruno C. Janegitz a,b *

a Laboratory of Sensors, Nanomedicine, and Nanostructured Materials, Federal University of São Carlos, 13600-970, Araras, SP, Brazil

b Department of Department of Natural Sciences, Mathematics and Education, Federal University of São Carlos, 13600-970, Araras, SP, Brazil

c Postgraduate Program in Chemistry, Federal University of Maranhão, 65080-805, São

Luís, MA, Brazil

d Department of Chemical Technology, Federal University of Maranhão, 65080-805, São

Luís, MA, Brazil.

* Corresponding author: brunocj@ufscar.br

Figure S1. Steps involved in the preparation of the filament, complete sensing platform, and QCT analysis containing real images of all apparatus utilized: (A) Component heating and homogenization, (B) Grinding of PP-PLA-CB conductive material pieces, (C) Extrusion of the PP-PLA-CB filament, (D) Printing of the electrochemical sensor and cell, (E) Representation of the electrochemical cell and (F) Electrochemical analysis of QCT.

Figure S2. DTG obtained for PLA, PP, copolymer (PP+PLA), CB, and the printed electrode.

Figure S3. RAMAN Spectra baseline corrected obtained for the printed electrode, with D and G bands highlighted

Figure S4. Wettability test by contact angle using 50 μL of deionized water obtained for CB-PP-PLA.

Figure S5. Equivalent circuits obtained for CB-PP-PLA sensor (A) untreated and (B) treated.

Figure S6. Square wave voltammograms obtained by CB-PP-PLA sensor, (A) in presence of QCT 10.0 mol L−1 in McIlvaine buffer 0.2 mol L−1 for pH values 2, 3, 4 and PB 0,2 mol L⁻¹ for pH values of 5, 6, 7, 8, 9 (SWV parameters: f = 25 mV, a = 20 mV and s = 2 mV); (A’) relation between current, potential and pH value; (B) f varying from 10 to 150 Hz (SWV parameters: f variable, a = 20 mV and s = 2 mV); (C) a varying from 10 to 150 mV (SWV parameters: f = 90 Hz, a variable and s = 2 mV); (D) s varying from 1 to 10 mV (SWV parameters: f = 90 Hz, a = 90mV and s variable), in the presence of QCT 10.0 μmol L−1 in McIlvaine buffer 0.2 mol L−1 (pH = 4); (B’) Insert f vs I; (C’) Insert a vs I; (D’) Insert s vs I.

Table S1. Comparison of fabrication strategies, materials, and surface pretreatment for 3D-printed sensors.

| Sensor | Polymer matrix | Conductive compound | Plasticizer | Solvent | Ambiental impact | Surface pretreatment | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- |
| G/AgNPs/PLA | PLA | Graphite and Ag nparticles | None | Acetone and chloroform | Very high | Polishing | [1] |
| Gpt/Al2O3/PLA | PLA | Graphite and alumina oxide | None | Acetone, chloroform and ethanol | Very high | Polishing | [2] |
| Gr-PLA | PLA | Graphite | None | Acetone, chloroform and ethanol | Very high | Polishing | [3] |
| CB-PLA | PLA | Carbon black | None | Acetone, chloroform and ethanol | Very high | Polishing and NaOH 0.5 mol L-1 activation | [4] |
| CB-PLA | PLA | Carbon black | None | 1,2-dichloroethane and acetic acid | High | Several (object of study) | [5] |
| CB-PLA-Oil | PLA | Carbon black | Soybean oil | None | Low | Polishing | [6] |
| Castor oil/rPLA | Recycled PLA | Carbon black | Castor oil | None | Low | Polishing and NaOH 0.5 mol L-1 activation | [7] |
| CB/ PI-PLA/PES | Post-industrial PLA | Carbon black | Polyethylene succinate (PES) | None | Low | Polishing and NaOH 0.5 mol L-1 activation | [8] |
| CB-G-PP | PP | Carbon black and graphite | None | None | Very low | Polishing and NaOH 0.5 mol L-1 activation | [9] |
| CB-PP-PLA | PP and PLA | Carbon black | None | None | Very low | Polishing | This work |

References

[1] N.M. Caldas, L.V. de Faria, A.G. Batista, A.O. Alves, S.C. Silva, D.A. Peixoto, et al., Graphite and silver nanoparticles-loaded polylactic acid matrix: A pioneering tailor-lab-made filament for manufacturing eco-friendly and robust electrochemical sensors towards pyridoxine detection, Electrochimica Acta, 504(2024) 144868.

[2] L.V. de Faria, N.M. Caldas, L.M. Villafuerte, S.F.L. do Nascimento, D.G.S. Quattrociocchi, T.d.M. Lima, et al., Graphite/Aluminum oxide/polylactic acid composite material: A valuable strategy for additively manufacturing cheap and improved electrochemical platforms for sensing sulfamethoxazole in honey samples, Electrochimica Acta, 495(2024) 144480.

[3] J.S. Stefano, L.R.G. e Silva, R.G. Rocha, L.C. Brazaca, E.M. Richter, R.A.A. Muñoz, et al., New conductive filament ready-to-use for 3D-printing electrochemical (bio) sensors: Towards the detection of SARS-CoV-2, Analytica Chimica Acta, 1191(2022) 339372.

[4] J.S. Stefano, L.R.G.e. Silva, B.C. Janegitz, New carbon black-based conductive filaments for the additive manufacture of improved electrochemical sensors by fused deposition modeling, Microchimica Acta, 189(2022) 414.

[5] T.G. Barbosa, D.N. Silva, M.M. Borges, S.O. Trindade, T.C. de Oliveira Cândido, A.C. Pereira, Influence of Surface Treatments on the Electrochemical Performance of Lab-Made 3D-Printed Electrodes,  Analytica2025.

[6] L.R.G. Silva, L.V. Bertolim, J.S. Stefano, J.A. Bonacin, E.M. Richter, R.A.A. Munoz, et al., New route for the production of lab-made composite filaments based on soybean oil, polylactic acid and carbon black nanoparticles, and its application in the additive manufacturing of electrochemical sensors, Electrochimica Acta, 513(2025) 145566.

[7] R.D. Crapnell, I.V.S. Arantes, M.J. Whittingham, E. Sigley, C. Kalinke, B.C. Janegitz, et al., Utilising bio-based plasticiser castor oil and recycled PLA for the production of conductive additive manufacturing feedstock and detection of bisphenol A, Green Chemistry, 25(2023) 5591-600.

[8] E. Sigley, C. Kalinke, R.D. Crapnell, M.J. Whittingham, R.J. Williams, E.M. Keefe, et al., Circular Economy Electrochemistry: Creating Additive Manufacturing Feedstocks for Caffeine Detection from Post-Industrial Coffee Pod Waste, ACS Sustainable Chemistry & Engineering, 11(2023) 2978-88.

[9] B. Ferreira, R.D. Crapnell, E. Bernalte, T.R.L.C. Paixão, C.E. Banks, Low-cost conductive polypropylene for electroanalysis in organic solvents using additively manufactured electrodes, Electrochimica Acta, 515(2025) 145680.